Supplementary Material 2

Experiment use-wear results table

| Pre-Experiment – low-power |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Striation Location |  | Striation Shape |  | Striation Orientation |  | Striation Density |  |  | Striation Length |  | Levelling |  | Pit Location |  | Pit Density |  | Rounding Location |  | Polish Location | Crushing Location |  | Fracture Location | Fracture Type | Manufacture Wear Present |
| All replicas |  | Covers |  | Shallow V, overlapping |  |  |  | Close |  |  | Long, intermittent |  | Y |  | Next to striations |  | Close |  | N/A |  | N/A | Sparse, axe surface |  | N/A | N/A | N/A |
| Pre-Experiment – high-power |  |  |  |  |  |  |  |
|  |  | Polish Type |  | Polish Density |  | Striation Location |  |  | Striation Shape |  | Striation Density |  | Striation Length |  | Pit Location |  | Pit Density |  | Manufacture Wear Present |  |  |
| All replicas |  | Flat, rough |  | Close |  | Polish, dense |  |  | wide |  | Dense |  | long |  | N/A |  | N/A |  | N/A |  |  |

| Splitting Wood – low-power |  |  |
| --- | --- | --- |
| Strikes | Striation Location | Striation Orientation | Striation Shape | Striation density | Striation length | Pit location | Pit Shape | Pit density | Rounding location | Polish location | Crushing location | Fracture location | Fracture type |
| 50 | 3 groups, blade edge | Perpendicular to blade, parallel to one another | Superficial, Narrow, U-shaped profile | Sparse, groups of 2-4 | Short | 3 groups, blade tip centre & corners | Narrow, superficial | Few, sparse | Highest topography of pits | Blade corners, limited | N/A | Corner of blade from dropping axe | Multiple, overlapping |
| 100 | 3 groups, blade edge, bifacial | Perpendicular to blade, parallel to one another | Superficial, narrow, U-shaped profile | Sparse, groups of 4-6 | Short | 3 groups, blade tip centre & corners | Narrow, superficial | Sparse | Highest topography of pits & fracture | Highest topography, corners, limited | N/A | N/A | N/A |
| 200 | 6 groups, blade edge, bifacial | Perpendicular to blade, parallel to one another | Superficial, narrow, U-shaped profile | Sparse | Short | 6 groups, blade tip. Largest in centre | Narrow, superficial | Sparse, close within groups | Highest topography of pits & fracture | Highest topography, corners, limited | N/A | N/A | N/A |
| 500 | Evenly along blade edges, bifacial | Perpendicular to blade, parallel to one another | Narrow, U-shaped profile | Close | Short | Along blade tip & edges | Narrow, superficial; wider combined pits | Sparse to close, densest in blade centre | Blade corners, high topography of pits & fractures | Highest topography, corners, limited | Sparse, separated, blade tip | Centre of blade tip | Dense group of pits |
| 1000 | Evenly along blade edges, bifacial | Perpendicular to blade, parallel to one another | Narrow, U-shaped profile | Close; densest in areas of previous 3 groups | Short | Along blade tip & edges | Narrow, superficial; wider combined pits | Close; densest in blade centre & top corner | Covers the blade corners | Blade corners | Narrow, superficial, sparse, separated blade tip | Centre of blade tip | Dense group of pits |
| 1500 | Evenly along blade edges, bifacial | Perpendicular to blade, parallel to one another; straight & diagonal for medium | Narrow, U-shaped profile | Close-dense; sparse for medium | Short; medium 5mm | Along blade tip & edges | Narrow; abrasion | Densest in the original 3 groups, edge damage 5mm onto blade edges | Blade tip, edges and largest areas on corners | Blade corners where rounded | Singular grains, blade edge & tip, sparse | Singular grains, blade edge & tip, sparse | Abrasion, edge damage 5mm on to blade edges |
| 2000 | Evenly along blade edges, bifacial | Perpendicular to blade, parallel to one another; straight & diagonal for medium | Narrow, U-shaped profile | Dense | Short; medium 5mm | Along blade tip & edges | Narrow, wide for combined pits; abrasion | Dense on tip, close on blade edges, 10mm onto edges | Blade corners; high topography of pits on tip | Blade corners & top of axe corner where rounded | Dense pits on blade edges & tip | Dense pits on blade edges & tip | Microfractures within dense groups of pits on blade tip & edges |

| Splitting wood – high-power |  |  |  |  |
| --- | --- | --- | --- | --- |
| Strikes | Polish type | Polish density | Polish development | Striation |  | Striation Shape | Striation density | Striation length | Pit location | Pit density | Manufacture wear present |
| 50 | N/A | N/A | No/undeveloped | N |  | N/A | N/A | N/A | N/A | N/A | No visible change to polish. No new use polish |
| 100 | Granular | Sparse, small patches | Undeveloped | N |  | N/A | N/A | N/A | N/A | N/A | Granular polish in between manufacture polish; manufacture polish smaller |
| 200 | Domed; singular polished grains | Partially connected patches; unconnected | Less developed | N |  | N/A | N/A | N/A | N/A | N/A | Sparse patches of granular polish, high topography domed |
| 500 | Domed, directionality | Partial connected small patches | Less developed | Y |  | Parallel, orientation matches polish directionality | Sparse; 2-3 striations in patches | short | N/A | N/A | Undeveloped appearance |
| 1000 | Domed, directionality perpendicular to blade edge | Small-moderate patches, close density | Less-moderate developed; undeveloped in between patches | Y, Cover domed patches |  | Parallel | Close | short | micro-pits on polish, tip | sparse | N |
| 1500 | Domed, directionality perpendicular to blade edge | Moderate sized patches, close density; singular in between | Less-moderate developed; undeveloped in between patches | Y, Cover domed patches |  | Parallel, orientation matches polish directionality | Close to dense | short | On more developed polish, blade edges, tip | Sparse | N |
| 2000 | Domed, directionality perpendicular to blade edge | Moderate sized, partially connected patches | Moderate | Y, Cover domed parches |  | Parallel; matches polish directionality | Close to dense | short | Larger patches of polish, blade edges, tip | close | N |

| Chopping Wood – low-power |  |  |
| --- | --- | --- |
| Strikes | Striation Location | Striation Orientation | Striation Shape | Striation density | Striation length | Pit location | Pit Shape | Pit density | Rounding location | Polish location | Crushing location | Fracture location | Fracture type |
| 50 | 3 groups, bifacial | Perpendicular to blade, parallel to one another | Narrow, u-shaped profile | Sparse | Short | 3 groups, blade tip centre & corners | Superficial, narrow | Sparse | High topography corners, limited | N/A | N/A | N/A | N/A |
| 100 | 4 groups, bifacial | Perpendicular to blade, parallel to one another | Narrow, u-shaped profile | Sparse to close | Short | 4 groups, blade tip | Superficial, narrow | Sparse to close; edge damage limited | Corners of blade tip, high topography | N/A | N/A | N/A | N/A |
| 200 | In groups covering most of blade edges, bifacial | Perpendicular to blade, parallel to one another; diagonal at blade corners | Narrow, u-shaped profile | Sparse to close | Short; up to 2mm; shortest at blade corners | 2mm onto blade edges, bifacial | Superficial, narrow but wider than 100 strikes | Close | High topography of pits on blade tip | High topography, blade corners | High topography; blade edge & tip centre; sparse | High topography; blade edge & tip centre; sparse | Microdamage |
| 500 | Covers most of blade tip & edges, bifacial | Perpendicular to blade, parallel to one another; diagonal at blade corners | Narrow, u-shaped profile | Close; Larger groups than previously | Short; 1-2mm | Covers most of blade tip and edges, bifacial | Narrow, superficial pits surround wider pits | Close | High topography of pits on blade tip | High topography, blade corners | Tip centre, sparse | High topography; blade edge & tip | Microdamage |
| 1000 | Continuous across blade tip & edges, bifacial | Perpendicular to blade, parallel to one another; diagonal at blade corners | Narrow, u-shaped profile | Close | 5mm onto blade edges, bifacial | 5mm onto blade edges, bifacial; larger clusters | Superficial, wide | Close; dense pits within wider clusters on tip | High topography of pits on blade tip | High topography, blade tip, towards corners | Within wider pit groups | Within wider pit groups | Edge scarring |
| 1500 | Continuous across blade tip & edges, bifacial | Perpendicular to blade, parallel to one another; diagonal at blade corners | Narrow, u-shaped profile | Close-dense | 5mm onto blade edges, bifacial | Continuous across blade tip & edges, bifacial | Wide; newer puts are superficial | Close, dense on tip where pit clusters extend across tip onto both blade edges | High topography of pits on blade tip | High topography along blade tip, sparse, wider towards corners | Within and around pit clusters on tip, and those extending onto blade edges | Within pit clusters on tip, and those extending onto blade edges | Edge scarring; microfractures; step fracture from axehead falling |
| 2000 | Continuous across blade tip & edges, bifacial | Perpendicular to blade, parallel to one another; diagonal striations cross other striations in centre & top corner of the blade edges. | Narrow, u-shaped, often interrupted by pits | Dense | 10mm onto blade edges, bifacial | Continuous across blade tip & edges, bifacial | Narrow, u-shaped; wider on tip than blade edge | Dense | High topography of pits on blade tip & flake negative | High topography of pits on blade tip & flake negative | Sparse, associated with pit clusters | Blade centre | Dense edge damage |

| Chopping wood – high-power |  |  |  |
| --- | --- | --- | --- |
| Strikes | Polish type | Polish density | Polish development |  | Striations | Striation Shape | Striation density | Striation length | Pit location | Pit density | Manufacture wear present |
| 50 | Rounded | Sparse | undeveloped |  | N | N/A | N/A | N/A | N/A | N/A | Present, altered with rounded edges |
| 100 | Domed | Separated Patches of sparse grains; small | Less developed |  | Y | Singular, overlapping | Sparse | Short | N/A | V/A | No further changes |
| 200 | Domed with slight directionality | Separated Patches of sparse grains; small | Less developed |  | Y | Parallel, orientation same as polish | Sparse | Short | Blade edges, largest polish patches | Sparse | Still visible |
| 500 | Domed, clear directionality | Small patches, partially connected | Less-moderate |  | Y | Parallel, orientation same as polish | Sparse | Short | Blade edges, tip, largest polish patches | Sparse | Still visible |
| 1000 | Domed, directionality; singular polished grains | Small sparse-close patches; sparse singular polished | Moderate; singular – less developed |  | Y | Parallel, orientated perpendicular to blade | Close | Short | Blade edges, tip, largest polish patches | Sparse | Still visible between use-polish |
| 1500 | Domed, directionality | Partially connected patches, dense on tip, particularly centre | Moderate |  | Y | Parallel, orientated perpendicular to blade | Close to dense | Short | Blade edges, tip, largest polish patches | Sparse | Significantly reduced |
| 2000 | Domed, smooth, clear directionality | Partially connected large patches | Moderate – well developed |  | Y | Parallel, orientated perpendicular to blade | Close | Short | Blade edges, tip, largest polish patches | Sparse to close | Undeveloped |

| Digging Soil with Stones – low-power |  |  |
| --- | --- | --- |
| Strikes | Striation Location | Striation Orientation | Striation Shape | Striation density | Striation length | Pit location | Pit Shape | Pit density | Rounding location | Polish location | Crushing location | Fracture location | Fracture type |
| 50 | Across blade edges, bifacial | Perpendicular to blade, parallel to one another | Narrow, superficial | Sparse | Long; up to 5mm on blade edge | 5 groups on blade tip & edges, centre & corners; up to 5mm on blade edge | Narrow, superficial | Clusters, moderate density | Blade tip centre, high topography | Blade tip centre, high topography | Grain removal pits, sparse | N/A | N/A |
| 100 | Across blade edges | Perpendicular to blade, parallel to one another, singular striations diagonal, overlapping | Narrow, superficial | Sparse; more numerous on one edge | Long & short, up 10mm onto blade edges | 5 groups on blade tip & edges, centre & corners; up to 5mm on blade edge | Superficial; groups gain width | Close, denser on tip; clusters along tip and blade edges, close to striations | High topography of pits | High topography, tip centre | Within pit groups, along striations | Within pit groups | Microfractures; frosted appearance |
| 200 | Across blade edges | Perpendicular to blade, parallel to one another & singular diagonal, overlapping | Narrow; singular wide striations & scratches | Close; Sparse scratches | Long & short; intermittent; between 8 & 20mm. | 5 groups on blade tip & edges, centre &corners; up to 5mm on blade edges | Angular, join to create group | Close-dense | Top blade corner, centre blade; high topography | Blade centre, high topography | Centre of blade tip & edges; along central striations | Centre of blade tip & edges | Microfractures; frosted appearance |
| 500 | Across blade edges | Perpendicular to blade, parallel to one another & singular diagonal, overlapping | Narrow, superficial; wide singular striations | Dense in centre, close elsewhere; sparse singular striations | Short from pits; long | Extend 20mm onto top corner blade edges, 10mm elsewhere | Abrasion at blade top corner | Close; close-dense in blade centre | High topography of tip, focus on bottom corner | Blade centre, high topography | Pits, blade edges & tip; focus on blade top corner | Pits, blade edges & tip | Overlapping flake negatives; microfractures, frosted appearance |
| 1000 | Across blade edges, bifacial | Perpendicular to blade, parallel to one another & singular diagonal, overlapping | Narrow, superficial; wide singular striations | Close to dense | Short; long, intermittent; 20mm onto blade edges | Blade tip & edges | Large clusters, angular, overlapping | Dense on tip; close elsewhere | High topography of tip, focus on bottom corner | High topography, blade corners, limited due to removals | Close, pits | Blade centre & top corner | Overlapping flake negatives |
| 2000 | Covers blade edges, bifacial | Perpendicular to blade, parallel to one another & singular diagonal, overlapping | Narrow, superficial; wide scratches & singular diagonal striations | Dense | Long, intermittent, interrupted by pits; extends to perforation at corners | Covers blade tip & edges | Narrow, angular clusters, overlapping | Dense, highest density at top & entre of tip, truncating tip | Blade corners; extend around the perforation | Blade corners; extend to perforation; areas of butt | Along tip and blade edge, concentrated within pits | Along tip & edges | Overlapping flake negatives, truncated tip |

| Digging soil with stones – high-power |  |  |  |
| --- | --- | --- | --- |
| Strikes | Polish type | Polish density | Polish development |  | Striations | Striation Shape | Striation density | Striation length | Pit location | Pit density | Manufacture wear present |
| 50 | Rounded | Sparse | Undeveloped |  | N | N/A | N/A | N/A | N/A | N/A | Present, altered with rounded edges |
| 100 | Granular | Separated patches, sparse | Undeveloped |  | N | N/A | N/A | N/A | N/A | N/A | Still clear, but reduced by new polish |
| 200 | Granular, no directionality | Separated patches, sparse | Less developed |  | Y | Narrow, singular, overlapping | Close | short | N/A | N/A | Visible but smoother through use |
| 500 | Granular | Close density | Less-moderate |  | Y, on tip | Narrow, singular, overlapping | Close | short | N/A | N/A | Noticeably altered; smoother |
| 1000 | Granular; smooth patches | ? Close-dense patches | Moderate |  | Y | Narrow, singular, overlapping | Close-dense | short | N/A | N/A | Visible but limited in size |
| 2000 | Smooth; granular | Large smooth connected patches | Moderate-well developed |  | Y | Narrow, singular, overlapping | Numerous, close-dense | short | N/A | N/A | Undeveloped |

| Digging Soil with Roots – low-power |  |  |
| --- | --- | --- |
| Strikes | Striation Location | Striation Orientation | Striation Shape | Striation density | Striation length | Pit location | Pit Shape | Pit density | Rounding location | Polish location | Crushing location | Fracture location | Fracture type |
| 50 | Blade corners | Perpendicular to blade, parallel to one another | Narrow, superficial | Sparse, groups of c.2 | Short | Blade tip, mostly corners | Small, superficial, narrow | Sparse | N/A | N/A | N/A | N/A | N/A |
| 100 | Blade edges, bifacial | Perpendicular to blade, parallel to one another; long overlap above | u-shaped, narrow, superficial | Sparse to close; groups of 6 | Short; few sparse long, intermittent blade centre | In 6 groups on blade tip & edges, more on edges than tip | Small, superficial | Sparse | Sparse & separated; high topography tip centre | N/A | N/A | N/A | N/A |
| 200 | Along blade edges, bifacial | Perpendicular to blade, parallel to one another; long singular overlap above | U-shaped profile, thin; wide singular scratches | Sparse, limited singular striations | Short; up 5-10mm | Small pits between 6 group | Narrow, superficial; wider edge damage directly next to blade tip | Sparse | Higher topography in blade centre | Sparse high topography on tip | N/A | Pits in blade centre | Microfractures |
| 500 | Concentrated to centre & top of blade | Perpendicular to blade, parallel to one another; diagonal, overlapping in centre | U-shaped, narrow, superficial; wider scratches | Close | Short, 2mm; long, intermittent 10-12mm | Blade centre & top of blade | Edge damage spread further onto edges, 2mm; superficial pits surround striations | Sparse to close on tip; close on blade edge | Blade corners | Blade edge centre, close to tip | N/A | Within pits on blade tip | Microfractures |
| 1000 | Partially even spread across blade edges | Perpendicular to blade, parallel to one another; diagonal, overlapping along blade edges | U-shaped, superficial, mixture of narrow and wider | Close | Long, intermittent striations, 15mm | Across tip & edges; pits apparent at bottom corner | Wide clusters extending onto blade edges, sparsely spread along tip; separated pits on blade edges | Sparse on edges, close in centre & top corner | Bottom blade corner | Partially connected, high topography on blade edges & tip | Separated, within pit clusters | Along tip, within pit clusters | Microfractures |
| 1500 | Evenly spread along blade edges | Perpendicular to blade, parallel to one another; diagonal, overlapping multiple directions | U-shaped, superficial, mixture of narrow and wider | Close to dense; densest in blade centre top corner | Long, intermittent; 10-20mm | Clusters 20mm wide; 15-20mm onto blade edges, more towards bottom corner | Superficial; Larger on & directly next to tip | Close to dense on tip, close on blade edges | High topography around pits on tip & edges | Separated, high topography on blade edges & tip | Blade centre | Blade centre | Microfractures; edge scarring |
| 2000 | Evenly spread along blade edges | Perpendicular to blade, parallel to one another; central diagonal striations overlap | Narrow, superficial, u-shaped; wider diagonal striations | Dense | Long, intermittent; 20mm | Blade tip & 20mm onto edges | Superficial, wide and shallow on tip | Close- dense; dense on tip & edge where striations overlap | Tip & blade edge; reducing visibility of pits on tip | High topography of tip & edge; location of rounding | Within dense pits | Within dense pits | Frosted appearance |

| Digging soil with roots – high-power |  |  |  |
| --- | --- | --- | --- |
| Strikes | Polish type | Polish density | Polish development |  | Striations | Striation Shape | Striation density | Striation length | Pits | Pit density | Manufacture wear present |
| 50 | Undeveloped | Separated, sparse | Undeveloped |  | Y | Narrow, singular, multi-directional | Sparse-close | Short | N/A | N/A | Present, altered by striations |
| 100 | Granular, slight rounding of edges | Sparse-close granular, sparse domed | Less developed |  | Y | Narrow, singular, perpendicular to blade | Close | Short | N/A | N/A | Present, reduced quantity |
| 200 | Granular; domed, slight directionality; rounded edges | Sparse granular; sparse to close domed, small patches | Less developed |  | Y | Narrow, singular, multi-directional | Close | Short, longer at blade centre | N/A | N/A | Present, reduced quantity |
| 500 | Granular; domed grains | Close, small partially connected patches | Less-moderate |  | Y | Singular, overlapping, multi-directional | Close | Short, longer at blade centre | Domed polish | sparse | Undeveloped |
| 1000 | Domed; granular | Close, partially connected patches; granular surrounding patches | Moderately |  | Y | Singular, overlapping, multi-directional | Close | Long | Domed polish | sparse | Undeveloped |
| 1500 | Domed with directionality; granular | Close, partially/more connected patches; granular surrounding patches | Moderately |  | Y | Singular, overlapping, multi-directional | Close-dense | Short and long | Domed polish | sparse | Undeveloped |
| 2000 | Domed; granular | Larger connected domed patches; granular surrounding | Well-devloped |  | Y | Singular, overlapping, multi-directional | Dense | Short andLong | Domed polish | Sparse-close | Undeveloped |

| Breaking Bone – low-power |  |  |
| --- | --- | --- |
| Strikes | Striation Location | Striation Orientation | Striation Shape | Striation density | Striation length | Pit location | Pit Shape | Pit density | Rounding location | Polish location | Crushing location | Fracture location | Fracture type |
| 50 | Top corner of blade, bifacial; surround pits. | Perpendicular to blade, parallel to one another | Narrow; superficial | Sparse | Short; 5mm | Along blade tip, extend slightly onto blade edges at blade corners | Superficial, narrow | Sparse, in groups | Close density patches, blade tip & 10mm onto edges | Close density patches, blade tip & 10mm onto edges | Within pits, separated & sparse | Within pits, separated & sparse | Microfractures |
| 100 | Extend across blade edges, bifacial; non-uniform | Perpendicular to blade, parallel to one another; larger at corners are diagonal, overlapping | Narrow; superficial | Sparse | Variable length; intermittent | High topography of blade tip & edges; 5mm onto edges | Superficial, narrow; blade edge centre abraded | Sparse- to close | High topography of blade tip & edges | High topography of blade tip & edges | Within separated pits on tip | Within separated pits on tip | Microfractures |
| 200 | Across blade edges; focus on blade corners | Perpendicular to blade, parallel to one another; larger at corners are diagonal, overlapping | Superficial, narrow; V-shaped | Close; sparse singular diagonal striations | Scratches 50mm onto blade edges; striations 10mm | More on blade edges than tip; 10mm onto edges | Superficial; narrow | Close on edges, sparse on tip | Blade tip, reducing pit density | High topography, blade & tip centre | Within pits on blade edges | Within pits on blade edges | Microfractures |
| 500 | Across blade edges; scratches on blade edges, close to tip | Perpendicular to blade, parallel to one another; singular, diagonal &overlapping | Superficial, narrow; V- shaped | Close; dense at corners | Long, intermittent; 10-20mm onto edges; overlapping striations starting from 20mm on one edge | 10-20mm onto edges | Superficial, narrow | Close, close-dense at corners | Blade tip, mainly corners; separated patches on centre blade edges | High topography, blade & tip centre | Clusters, within pits on tip and amongst striations on blade edges; sparse | Within pits on tip and amongst striations on blade edges; sparse | Microfractures |
| 1000 | Across blade edges, starting at tip & from 10mm on blade edges | Perpendicular to blade, parallel to one another; diagonal long striations overlap. | Superficial, narrow | Close | Short parallel; long, intermittent overlapping; 10-30mm | Along tip & 10-30mm onto edges, around striations | Superficial; narrow; wider in tip centre | Close | 5mm onto blade edges | High topography, blade & tip centre and top corner | Clusters in blade edges starting from 10mm | Centre of tip; clusters in blade edges starting from 10mm | Microfractures |
| 1500 | Almost even spread along blade edges; long striations start from 10mm on blade edges | Perpendicular to blade, parallel to one another; diagonal long striations overlap. | Superficial, narrow; wide diagonal striations | Close | Short parallel; long, intermittent overlapping; 10-20mm | Along tip & 10-20mm onto edges, around striations | Superficial; narrow; wider in tip centre | Close | Tip & 15mm onto blade edges; high topography of blade corners | Blade corners, rounded grains in blade centre | Within long striations | Blade tip centre | Microfractures |
| 2000 | Covers blade edges, concentration at corners and centre of blade; scratches parallel to tip | Perpendicular to blade, parallel to one another; diagonal, long singular striations overlap | Superficial, narrow; scratches, long striation are wider | Close; close to dense at blade corners | Short parallel; long, intermittent singular 25mm onto blade edges; long scratches | 25mm onto blade edges | Superficial, narrow; wide on/close to tip | Close; close-dense on/close to tip | Tip, reducing size of pits; edges of pits | Blade corners, limited in blade centre | Separated patches 2-4mm onto blade edges | Close patches 2-4mm onto blade edge; interrupt pits | Microfractures; frosted appearance |

| Bone Breaking – high-power |  |  |  |
| --- | --- | --- | --- |
| Strikes | Polish type | Polish density | Polish development |  | Striations | Striation Shape | Striation density | Striation length | Pits | Pit density | Manufacture wear present |
| 50 | N/A | N/A | N/A |  | N | N/A | N/A | N/A | N | N/A | No change to manufacture polish |
| 100 | Undeveloped | Undeveloped | Undeveloped |  | N | N/A | N/A | N/A | N | N/A | Partially altered, smoother |
| 200 | Smooth, rounding of edges | Close, partially connected patches | Less-moderate |  | Y | Parallel and singular, overlapping | Sparse | Short | N | N/A | Still visible |
| 500 | Smooth, slight rounding | Close, partially connected patches | Moderate |  | Y | Parallel arrangement; some diagonal & overlapping | Sparse, 5-6 on each patch | short | N | N/A | Less developed |
| 1000 | Smooth, rounded edges | Close, more numerous patches | Moderate |  | Y | Parallel arrangement, some diagonal & overlapping | Sparse-close; 5-10 on each patch | Short and long | Polish patches, tip and blade edge | close | Less developed |
| 1500 | Smooth, rounded edges | Close density, larger patches | Moderate-well developed |  | Y | Parallel, occasionally overlapping | Close-dense | Short and long | All polish | Close | Undeveloped |
| 2000 | Smooth, rounded edges | Close-dense | Moderate-well developed |  | Y | Parallel and singular, occasionally overlapping | Dense | Short and long | All polish | Close | N/A |

| Wedge Splitting Wood – low-power |  |  |  |
| --- | --- | --- | --- |
| Strikes | Striation Location | Striation Orientation | Striation Shape |  | Striation density | Striation length | Pit location | Pit Shape | Pit density | Rounding location | Polish location | Crushing location | Fracture location | Fracture type |
| 50 | Blade edge corners | Singular, perpendicular to blade tip | Short, superficial, narrow, u-shaped profile |  | Separated; variable density on each blade edge | 5-10mm | Blade edge corners; butt, off-centre | Superficial, narrow | Separated; variable density on each blade edge | N/A | N/A | N/A | N/A | N/A |
| 100 | 4 groups on blade edges, bifacial | Singular, diagonal & perpendicular to blade tip | Short, superficial, narrow, u-shaped profile |  | Sparse; denser in blade centre | Short & long; 10-15mm onto blade edges | 4 groups 10-15mm onto blade edges, bifacial | Superficial, narrow, wide, shallow on butt | Sparse on blade edges; close near to/on tip | Sparse, centre of blade tip | Rounded areas | Blade edge, close to tip | Within close groups of pits, concentration in blade centre | Microfractures |
| 200 | Across blade tip & edges | Singular, diagonal & perpendicular to blade tip, overlap | Short, superficial, narrow, u-shaped profile |  | Sparse, denser at blade corners | Short & long; 10-15mm onto blade edges | Across blade tip & edges; butt centre | Superficial, narrow; superficial, wide on butt | Sparse, denser at blade corners | Sparse, blade corners | Blade corners | Cluster at one blade corner | Clusters, butt centre | Microfractures |
| 500 | Across blade tip & edges; from centre to edges of butt | Singular & parallel striations, multi-directional, overlap on blade & butt | Short, superficial, narrow, u-shaped profile & narrow on butt |  | Close; sparse further away from tip | Long, 15mm onto blade edges, intermittent; short on butt | Tip; 15mm onto blade edges; 5 groups on butt, from centre to edges | Superficial | Close; sparse further away from tip | Sparse, blade tip | Blade tip, centre and corners | Blade edge, directly next to tip, centre and corners | Clusters on tip, extending onto blade edges | Microfractures |
| 1000 | Cover blade edges, across butt | Perpendicular to blade, parallel to one another; diagonal, singular striations overlap in blade centre; parallel, multi-directional on butt | Short, superficial, narrow, u-shaped profile |  | Close; Close-dense at corners | Long, 20mm onto blade edges; short, slightly diagonal striations begin after 10mm on edges | Tip; 20mm onto blade edges, across butt | Superficial; linear patches on blade edges; wide on butt | Close; Close-dense at corners | High topography along blade edges up to 10mm; rounding on high topography of butt | Rounded areas on blade edges | Blade edges with focus on centre of blade. centre of butt | Within linear patches, most dense on tip; dense in butt centre | Microfractures |
| 1500 | Cover blade edges, concentration of overlapping in blade centre | Perpendicular to blade, parallel to one another; diagonal & overlap in blade centre & butt | Short, superficial, narrow, u-shaped profile |  | Close to dense on blade & butt | Intermittent, 20-25mm onto blade edges | 20-25mm onto blade edges | Superficial, narrow, further away from tip | Close-dense on blade & butt; wider groups, wide pits | High topography, blade & tip & of pits more heavily rounded | Rounded areas on blade edges | Large clusters centrally on blade tip & edges | Surrounding pits | Microfractures |
| 2000 | Cover blade edges; mostly covers butt | Perpendicular to blade, parallel to one another; diagonal & overlap in blade centre & butt | Superficial; deeper in blade centre |  | Close to dense on blade & butt, denser at blade corners | Short & medium, intermittent, up to 30mm onto blade edges | 30mm onto blade edges; mostly covers butt | Superficial, narrow; wider pits on & directly next to tip | Close on blade & butt; close-dense wide clusters in tip centre & corners; sparse to sparse-close further from tip | High topography, blade edges and more heavily rounded on tip & pit edges more; partially connected on high topography across butt | rounded area, with focus directly next to and on tip | Centrally on butt | Centrally on blade edges, along deep striations | Irregular patches, 5x5mm; frosted appearance |

| Wedge splitting wood – high-power |  |  |
| --- | --- | --- |
| Strikes | Polish type | Polish density |  | Polish development | Striations | Striation Shape | Striation density | Striation length | Pits | Pit density | Manufacture wear present |
| 50 | N/A | N/A |  | N/A | N/A | N/A | N/A | N/A | N/A | N/A | Visible, unchanged |
| 100 | Granular | Separated, sparse |  | Undeveloped | N | N/A | N/A | N/A | N | N/A | Present; interrupted by use-polish |
| 200 | Domed, granular | Sparse on blade & butt; close within patches of domed & granular |  | Less developed | N | N/A | N/A | N/A | N | N/A | Present; edges rounded from use |
| 500 | Domed, directionality | unconnected patches on tip, close, partially- connected on blade edges & butt |  | Less developed | Y | Parallel arrangement on butt & blade in same direction as polish directionality | Sparse | Short | Polish on butt | sparse | Present, edges rounded |
| 1000 | Domed, directionality parallel with & also perpendicular and parallel to blade | Close on blade edges, tip & butt |  | Moderate | Y | Parallel arrangement on butt & blade in same direction as polish directionality; slightly overlapping on butt | Close | Short | Polish on butt & blade edge | sparse | Undeveloped close to tip |
| 1500 | Domed, directionality | Close; larger patches on blade & butt |  | Moderate | Y | Parallel arrangement on butt & blade in same direction as polish directionality; slightly overlapping on butt | Close | Short | Polish on butt & blade edge | sparse | Undeveloped |
| 2000 | Domed, directionality | Close, partially connected small and larger patches, interrupted by grain removal |  | Moderate-Well developed | Y | Parallel arrangement on butt & blade in same direction as polish directionality; slightly overlapping on butt | Close-dense | Short | Polish on butt & blade edge | Sparse-close | N/A |