# Biomass-derived mesoporous core-shell Fe3C@graphene

3

oxide nanospheres for electrochemical energy storage

4

5

6

7	Xinli Yi,a,b Wen He,c* Xudong Zhang,c Kwan San Huid and Wangwang Xua*

8

9

10

11	a.College of Materials and Chemical Engineering, Key Laboratory of Inorganic

12

13	Nonmetallic Crystalline and Energy Conversion Materials, China Three Gorges

14

16

15	University, Yichang, 443002, P. R. China

18

17	b.Hubei Three Gorges Laboratory, Yichang, Hubei 443007, P. R. China.

20

19	c.Department of Materials Science and Engineering, Qilu University of Technology

21

22	(Shandong Academy of Sciences), Jinan, 250353, P. R. China.

23

24	d.School of Engineering, Faculty of science, University of East Anglia, Norwich, NR4

25

26	7TJ, United Kingdom.

27

28

29

30

31	Abstract

32

33

34	The biomass-derived mesoporous core-shell Fe3C@graphene oxide nanospheres

35

36	(mFe3C@GO NSs) was synthesized with high-quality lignins and applied for

37

38	electrochemical energy storage. The synthesis conditions of mFe3C@GO NSs are

39

40	optimized and   its formation   mechanism   is   proposed.   The mFe3C@GO   NSs

41

42	homogeneously dispersed in GO conductive network and maintained the structural

43

44	integrity of the electrode in the electrochemical process. Benefiting from the

45

47

46	advantages   of   the   core-shell   construction   and   graphene   oxide   network,   the

49

48	mFe3C@GO NSs exhibits extensible exploration in electrochemical energy storage

50

51	(EES).

52

53	Keywords:	mFe3C@GO	NSs;	Biomass-derived	compounds;	Nanostructured

54

55	electrode; Lithium-ion battery; Electrochemical energy storage

56

57

58

## 1	1. Introduction

2

3	By integrating Li-ion battery electrode and supercapacitor into one device is

4

6

5	expected to combine the advantages of the two energy storage mechanisms to

8

7	obtain  a  “double  high”  Li-ion  battery  (LIB)  and  supercapacitor  (SC)  hybrid

9

10	energy  storage  devices  (LIB-SC  HESDs),  which  are  likely  to  be  the  future

11

12	power   source   for   multi-function   electronic   equipment   and   electric/hybrid

13

14	vehicles [1, 2]. However, the performance of LIB-SC HESDs is limited by the

15

16	mismatched	charge	storage	capacity	and	electrode	kinetics	between

17

18	battery-type	and	capacitive	electrodes	[1].	Therefore,	the	design	of

19

20	high-performance   electrode   materials   and  understanding   on   the  matching

21

23

22	theory  between  the  positive  and  negative  electrodes  of  LIB-SC  HESDs  face

25

24	overwhelming challenges [3].

26

27	Graphene (GN)-like two-dimensional (2D) materials have the potential in

28

29	applications due to their unique interfacial structure, attractive properties, facile

30

31	synthesis, and ease of functionalization [4, 5]. Numerous studies indicate that

32

33	the	effective	work	function	of	carbon-based	electrode	was	increased

34

35	significantly  by  inserting  metal  oxide  nanoparticles  [6-8].  The  GN  and  iron

36

37	carbide  (Fe3C)  bifunctional  oxygen  electrocatalysts  demonstrated  synergistic

38

40

39	effects  [9,  10].  Fe3C  was  applied  in  lithium-ion  batteries  (LIBs)  as  anode

42

41	material, the question remains, however, the structure collapse originating from

44

43	volume  change  during  the  continuous  charge/discharge  process  and  the  poor

45

46	conductivity  of  Fe3C  resulted  in  rapid  capacity  fading,  particularly  in  high

47

48	current density [11]. Structure engineering and conductive network doping had

49

50	wide	applicability	to	solve	these	problems	[12-14].	Nevertheless,	the

51

52	fabrication of core-cell carbon coating with different design strategies of large

53

54	specific surface area, excellent conductivity and mechanical flexibility lead to

55

56	restricted performance improvement [15]. In general, the core-shell structure is

57

58	desirable to realize synergism effect, but surprisingly little attention focus on

1	the  utilization  of  lignin.  Lignin  emerges  as  a  by-product  from  papermaking

2

3	industry  by  the  degradation  of  the  nature   wood,   which  is   suitable  for

4

5	thermochemical  reaction  for  its  high  yield  of  pyrolysis  products  and  is

6

7	considered a promising feedstock for carbon materials production [16, 17]. Its

8

9	surfactant   structure   contains   multifarious   functional   groups   of   carboxyl,

10

11	hydroxyl, benzyl alcohol, methoxyl, and trace elements (such as Si and S, etc),

12

13	providing lone pair electrons, nucleation sites and adsorb metal ions [18].

14

16

15	Here,  the  biomass-derived  mesoporous  core-shell  Fe3C@graphene  oxide

18

17	nanospheres  (mFe3C@GO  NSs)  were  fabricated  by  a  simple  wet  chemical

20

19	route with  high-quality  lignins  as the  organic  ligands  of Fe(II)/Fe(III)-MOFs

21

22	precursor and the carbon source, and the synthesis mechanism was proposed.

23

24	The microstructure and chemical composition exhibits synergetic effects of fast

25

26	ion insertion/extraction, high electrolyte permeability, and electric conductivity

27

28	for lithium-ion battery and supercapacitor, respectively. More importantly, the

29

30	HESDs  constructed  with  mFe3C@GO  NSs  and  mesoporous  Li3V2(PO4)3/C

31

32	microspheres   (mLVP/C   MSs)   [19]   exhibit   highly   matched   capacity   and

33

35

34	significant pseudocapacitive behavior.

36

## 37	2. Experiments sections

38

39

## 40	2.1. Synthesis of mFe3C@GO NSs

41

42	The Fe3O4-MOFs precursor was synthesized by a simple, low-cost and green method

43

44	of hydrothermal crystallization and reduction. Typically, 33 mL 1mol L−1 Fe3+

45

46	solution was slowly added into 50 mL lignin solution with magnetic stirring for 6 h at

47

48	room temperature to form a thick liquid. The pH value of the mixed solution was

49

50	reduced from 13 to 7. Subsequently, the mixed solution was shifted to a Teflon-sealed

51

52	autoclave and heat-treated for 48 h at 180°C. After the autoclave cooled down to room

53

54	temperature naturally, the precipitate was washed with deionized water for three times

55

56	and dried at 60 °C to obtain the Fe3O4-MOFs precursor. The mFe3C@GO NSs was

57

58	obtained by carbonizing Fe3O4-MOFs precursor at high temperature for 8 h in a tube

furnace with a heating rate of 5°C min−1 in nitrogen (N2) atmosphere. For comparison,

1

2	the GO blank sample was prepared without additional Fe3+ through similar conditions.

3

5

4	2.2. Characterizations

7

6	X-ray diffraction (XRD) was recorded on a LabX XRD-6100 with Cu-Kα radiation

9

8	(Shimadzu, λ= 1.5406 Å). X-ray photoelectron spectroscopy (XPS, ESCALAB Xi+)

11

10	was carried out to characterize the elemental components and chemical states of

13

12	elements. Field emission scanning electron microscopy (FE-SEM) was used to

14

15	observe the morphological structure of sample by a ZEISS scanning electron

16

17	microscope equipped with an X-ray energy dispersive spectrometer (EDS) at 20 kV,

18

19	and the EDS images were captured for analysing the distribution of elements. The

20

21	JEF-2100F is a transmission electron microscopy (TEM) that performed the lattice

22

23	fringe images under the condition of 200 kV. Raman spectra were measured by a

24

25	Renishaw RM2000 Raman microscope with 514 nm excitation argon laser.

26

27	Differential scanning calorimetry (DSC-100H, Nanjingdazhan) was used to measure

28

29	the thermal change of Fe3O4-MOFs precursor. The N2 adsorption–desorption isotherm

30

31	and Barrett–Joyner–Halenda (BJH) pore size distribution were obtained at 77 K using

32

33	an automatic surface area analyzer (Micromeritics, Gemini V2380, USA).

34

36

35	2.3. Electrochemical measurements

38

37	2.3.1 Li-ion batteries

40

39	The electrochemical performances were characterized in a coin-type LIR2032 cell at

42

41	room temperature. The working electrode was prepared by mixing 80% mFe3C@GO

44

43	NSs, 10% acetylene black and 10% polyvinylidene fluoride (PVDF) in N-methyl

45

46	pyrrolidone to prepare , and then the slurry was coated on copper foil surface

47

48	uniformly. After that, the electrode was dried at 60 °C in an electric thermostatic

49

50	drying oven and then dried at 110 °C for 10 h in vacuum drying oven. The electrode

51

52	was cut it into wafers with a diameter of 15 mm. The cells were assembled in a

53

54	high-purity argon-filled inert glove box with the synthesized electrode as anode and

55

56	polypropylene (PP) membrane as a separator, 1.0 M LiPF6 EC: DC: EMC (ethylene

57

58	carbonate: dimethyl carbonate: cthylene methyl carbonate = 1:1:1 ) as the electrolyte.

59

60	After	assembling	battery	pack	and	ageing	treatment,	the	electrochemical

characteristics were conducted. The charge-discharge and cyclic voltammetry (CV)

1

2	curves were measured by Channels battery analyzer (CT3008W) between 0.01–3.00 V.

3

5

4	Electrochemical impedance spectroscopy (EIS) tests were performed in the frequency

7

6	range from 100 KHz to 10 mHz. The CV and EIS measurements were recorded on a

9

8	PARSTAT 2263 electrochemical workstation. All the processes were measured at

11

10	room temperature.

12

## 13	2.3.2 Hybrid energy storage devices (HESDs)

14

15	Hybrid energy storage devices (HESDs) were constructed using mFe3C@GO NSs as

16

17	the anode and mLVP/C MSs as the cathode. The average mass loading of the mLVP/C

18

19	MSs cathode was about 1.35 mg cm−2. The charge-discharge curves were carried out

20

21	between 0.00–4.00 V. All the tests were performed at room temperature.

22

23	The average mass loading of the active material is shown in equation 1:

24

25	Mass load = m/A	1

26

27	Where m (mg) is the mass of active material, A (cm2) is the area of the electrode

28

29	sheet with a diameter of 15 mm.

30

31

## 32	3. Results and discussion

33

34

35

36

37

38

39

40

41

42

43

44

45

46

47

48

49

50

51

52

54

53	Fig.  1  (a-c)  Schematic  illustration  for  reaction  of  lignin  with  Fe3+.  (d,  e)

- Secondary building  units  of  Fe(III)-MOFs,  Fe(II)/Fe(III)-MOFs  and  spiral

57

Fe3O4-MOFs (gray: C; voilet: FeO6 octahedron; blue: FeO4 tetrahedron). (f)

58	Structure illustrations of mFe3C@GO NSs after carbonization.

59

60

1	Fe3+  is  an  ideal  metal  ion  to  construct  nodes  of  metal-organic  frameworks

2

3	(MOFs) due to its low toxicity, abundance and hard Lewis acid, resulting in

4

5	stronger coordinating bonding with organic ligands, and therefore more stable

6

7	frameworks [20-22]. The in-situ synthesis of mFe3C@GO NSs is shown in Fig.

8

9	1. Benefiting from Fe3+ ions and functional groups in lignin, the nucleation and

10

11	growth  of  the  lyotropic  liquid  crystals  (LLCs)  is  determined  (Fig.  S1a).

12

13	Moreover, the factor affecting the spontancous chelation and depolymerization

14

16

15	is electrophilic attack of lignins (Fig. 1a). The nucleation and growth of Fe3+

18

17	ions are correlated with the functional groups and highly hydrophilic groups on

20

19	lignin surface (Fig. 1b). When Fe3+ ions are deficient, the Fe/lignin chelates

21

22	tend to curl in some directions because of electrostatic attraction (Fig. 1c). The

23

24	hydrothermal crystallization behaviour of Fe(III)-MOFs in connection with the

25

26	self-assembly of Fe/lignin chelates. Surplus functional groups were pulled away

27

28	from the lignin structure and donated electron, causing the oxidation-reduction

29

30	reactions of Fe3+ ions and forming the Fe(II)/Fe(III)-MOFs, and ultimately the

31

32	spiral Fe3O4-MOFs (Fig. 1d  and e). In the synthesis process, Fe3O4 produce

33

35

34	chemisorption	to	the	π	bond	of	unsaturated	hydrocarbons	in	lignin,

37

36	consequently weakening the bond energy of lignin and prompting the cleavage

38

39	of  organo-functional  groups  (C-H  and  C-O  bonds).  Meanwhile,  the  lignins

40

41	provide carbon-rich matrix and abundant free carbon atoms. The mFe3C@GO

42

43	NSs was obtained by carbonizing Fe3O4-MOFs at 800 °C for 8 h in an nitrogen

44

45	atmosphere. Fe3C nanospheres that coated by graphene oxide are dispersed in

46

47	the conductive network of GO nanosheet homogeneously (Fig. 1f).

48

49	X-ray  diffraction  (XRD)  patterns  of  the  samples  synthesized  with  the

50

52

51	different addition amounts of Fe3+ were displayed in Fig. S2, demonstrating the

54

53	optimal volume ratio 0.66 of 1mol L−1 Fe3+ solution and the liquid containing

56

55	the lignin. The semi-transparent 3D visualisation image in Fig. 2a shows the

57

58	layered  skeleton  structure  and  open  interlinking  pores  of  Fe3O4-MOFs  with

59

60	oversize connected pores (0.5–1.0 μm) (Fig. S3). The X-ray diffraction (XRD)

1	pattern  demonstrates  the  crystal  structure  of  Fe3O4-MOFs  (Fig.  2b).  The

2

3	diffraction peaks at 5-30° correspond to the simulated MIL-53(Fe), while the

4

5	peaks at 30-80° relate to the Fe3O4 crystalline phase (JCPDS, No. 89-3854) [23,

6

7	24].  The  synthetic  temperature  of  Fe3C  range  from  750  to  850  °C  was

8

9	confirmed	by	differential	scanning	calorimeter	(DSC,	Fig.	S4).	The

10

11	mFe3C@GO NSs synthesized at 800 °C for 8 h is well indexed to orthorhombic

12

13	phase   of   Fe3C   (PDF#65-2413)   and   graphene   oxide,   while   the   samples

14

16

15	synthesized  at  750  °C  and  900  °C  contain  impurity  phase  (Fig.  2c).  The

18

17	graphene oxide with a high degree of disorder is evidenced by a wide reflection

20

19	2θ range from 20 to 30°, with a strong peak characteristic at 2θ=25°. Raman

21

22	spectra (Fig. 2d) indicate the intensity ratio (IG/ID=1.87) of mFe3C@GO NSs is

23

24	higher  than  that  of  GO  (IG/ID=1.06),  demonstrating  the  higher  graphitization

25

26	degree of graphene oxide in mFe3C@GO NSs. Furthermore, the sharper shape

27

28	and  stronger  intensity  of  2D  peak  for  mFe3C@GO  NSs  shifted  to  lower

29

30	frequency obviously, which may be result from the catalytic effect of Fe ions on

31

32	the cross-linking reaction of lignins and the graphitization of graphene in the

33

35

34	synthesis process.

37

36	X-ray photoelectron  spectroscopy  (XPS)  was  carried out to  characterize

38

39	the elemental components and chemical states of mFe3C@GO NSs (Fig. S5a).

40

41	High resolution XPS spectrum of Fe 2p present two signals at 711.5 eV (Fe

42

43	2p2/3)  and  726.0  eV (Fe  2p1/2),  declaring  that  Fe  is  in  a  CFe6  octahedron

44

45	environment with +1 valency (Fig. S5b) [13, 14]. The typical C-C peak and

46

47	C=C peak at 284.8 eV and 285.4 eV can be ascribed to the GO layer (Fig. S5c).

48

49	The  high-ordered  GO  nanosheets  was  formed  by  cross-linking  condensation

50

52

51	polymerization of lignin molecules during the heat treatment process.

54

53	The blank sample demonstrates the existence of GO and microcomponent

56

55	of SiC (Fig. 2c), in conjunction with a porous sponge structure (Fig. S6), in

57

58	which  graphene  oxide  nanosheet  interwined  closely  with  amorphous  carbon

59

60	(AC) and graphite carbon nanofibers (GCNFs). The 3D honeycomb structure of

1

2

3

4

5

6

7

8

9

10

11

12

13

14

15

16

17

18

- Fig. 2 (a) Local semi-transparent 3D visualisation image and (b) XRD patterns

21

of Fe3O4-MOFs precursor and simulated MOF-53(Fe). (c) XRD patterns. (d)

- Raman spectra. (e) TEM image and (f) the  elemental  mapping image of  Fe

- element. (g) TEM image and TEM-EDS line scan curves along the diameter

24

25	(the yellow line) of the mFe3C@GO NSs nanoparticle.

26

27

28

29	mFe3C@GO NSs (Fig. S7) composed of overlap nanosheets and nanospheres

30

31	exhibits	similar	morphology	to	Fe3O4-MOFs,	illustrating	the	structure

32

33	stabilization	without	collapse	during	calcination	process	owing	to	its

34

35	thermostability. TEM images (Fig. S8a-c) show different size of Fe3C core-shell

36

37	(10-100 nm) with a shell thickness of approximately 4.0 nm embedded in GO

38

40

39	nanosheets  uniformly.  The  lattice  spacings  of  0.20  and  0.24  nm  are  in

42

41	conformity to the (031) and (210) planes of Fe3C, respectively (Fig. S8d and e).

43

44	The  elemental  mapping  image  of   mFe3C@GO  NSs   indicate  the   weight

45

46	percentage  of  Fe  is  approximately  43%  (Fig.  2e  and  f).  The  elemental  line

47

48	scanning (Fig. 2f) reveal that the Fe element reduced gradually from core to

49

50	surface along the diameter of mFe3C@GO NSs nanosphere, further verifying

51

52	the inner core of Fe3C NPs are well coated by GO shells and homogeneously

53

54	dispersed in the conductive network of GO nanosheet (Fig. S9). Furthermore,

55

57

56	the increased intensity of ordered hierarchical mesopores conduces to improve

59

58	physical  and  chemical  properties  of  mFe3C@GO  NSs.  Most  notably,  the

60

1	mFe3C@GO  NSs  exhibit  an  ultra-high  BET  surface  area  of  639.1  m2  g−1,

2

3	promoting   the   permeability   of   electrolyte   and   resulting   in   an   excellent

4

5	electrochemical performance (Fig. S10).

6

7	Particularly,  the  mFe3C@GO  NSs  synthesized  at  800  °C  delivers  an

8

9	ultrahigh initial discharge capacity of 1800 mAh g−1 at the current density of 1

10

11	A g−1 and and remains at 800 mAh g−1 even at a high current density of 10 A g−1,

12

13	displaying superior high rate capability than that of other anodes for lithium-ion

14

16

15	battery (Fig. 3a). Charge/discharge voltage profiles of mFe3C@GO NSs at 1 A

18

17	g−1 remain the same and stable after 2nd cycle (Fig. S11), in conjunction with

20

19	the long term cycling performance at 10 A g−1 displayed in Fig. 3b. After 1000

21

22	cycles, the reversible capacity retention of mFe3C@GO NSs decreases to about

23

24	715 mAh g−1 and closes to the coulombic efficiency of 100%, demonstrating

25

26	the	outstanding	cycling	stability.	The	unique	core-shell	structure	of

27

28	mFe3C@GO NSs is conductive to provide abundant sites and  flexible buffer

29

30	space for Li+ storage. The prominent decreased peak intensity at 0.8 V after

31

32	1000th cycle and the disappeared peak at 1.5 V can be related to the irreversible

33

35

34	side reactions and the solid electrolyte interface (SEI) formation, respectively

37

36	(Fig. 3c). The charge transfer resistance (Rct) of mFe3C@GO NSs after 1000th

38

39	cycle indicates the improved ions and electrolyte transport properties (Fig. S12),

40

41	in accordance with the electronic conductivity.

42

43	The	hybrid	energy	storage	devices	(HESDs)	were	assembled	by

44

45	mFe3C@GO NSs (anode) and mLVP/C MSs (cathode) to reveal the potential

46

47	application.  The  anode/cathode  prelithiation  is  carried  out  to  overcome  the

48

49	electrolyte-consuming  problem,  tuning  the  electrochemical  performance  and

50

52

51	achieving remarkable energy and high power density [25, 26]. By contrast, the

54

53	luminosity  of  LED  bulb  driven  by  HESDs  after  prelithiation  (Fig.  3e)  is

56

55	significantly higher than that of LED bulb before prelithiation (Fig. 3d). The

57

58	HESDs  after  prelithiation  exhibit  better  rate  capability  (Fig.  3f).  The  initial

59

60	charge and discharge capacities after prelithiation are 544.7 and 528.1 mAh g−1

1

2

3

4

5

6

7

8

9

10

11

12

13

14

15

16

17

18

19

20

21

22

23

24

- Fig. 3 (a) Rate capability of electrodes synthesized at different temperature. (b)

- Cycling performance and Columbic efficiency of mFe3C@GO NSs. (c) Cyclic

28

voltammogran curves  at  the  scan  rate  of  0.1  mV  s−1.  Electrochemical

- performance	evaluation	of	HESDs	with	the	optimal	mass	ratio	of

- mpositive/mnegative=4.15. (d, e) Brightness contrast photos of LED bulb driven by

32

HESDs, (f) Rate performance, (g) Long-term cycling performance, (h) Nyquist

33	plots and (i) Ragone plots.

34

35

36

37	at 0.1 A g−1, respectively. The HESDs after prelithiation delivers excellent rate

38

39	performance at the rates from 1 to 5 A g−1, and the discharge capacity of 217.8

40

41	mAh g−1 can be remained at 5 A g−1. The long-term cycling performance of

42

44

43	HESDs after prelithiation is improved tremendously (Fig. 3g) in contrast to that

46

45	of HESDs before prelithiation, which can be attributed to lower Rct  (152.7 Ω)

47

48	(Fig.  3h)  and  the  enhanced  contribution  of  pseudocapacitive  behavior  (Fig.

49

50	S13).  Extraordinarily,  the  HESDs  after  prelithiation  still  display  a  discharge

51

52	capacity of 136 mAh g−1 and a retention rate of 91.6% after 1200 cycles at 5 A

53

54	g−1. The HESDs after prelithiation present ultrahigh energy and power densities

55

56	(Fig. 3i), exhibiting exceptionally matched faradaic capacity and kinetics.

57

58

59

60

1

2

3

4

5

6

7

8

9

10

11

12

13

14

15

16

17

18

19

21

20	Fig. 4 (a) CV curves, (b) Plots of log (sweep rate) versus log (peak current) and

- (c) Capacitive contribution of HESDs after prelithiation at various sweep rates.

- (e)  Schematic   diagram   of   energy   storage   mechanisms   of   HESDs   after

24

- prelithiation. Schematic representation of the microstructure of (d) batter-type

- mLVP/C MSs electrode and (f) mFe3C@GO NSs pseudocapacitive electrode.

27

28

29

30	The synergy effect between cathode and anode was further investigated to

31

32	explore  the  energy  storage  mechanism.  CV  curves  of  the  HESDs  after

33

35

34	prelithiation in a voltage window of 1.5-3.0 V with changing scanning rate from

37

36	0.2  to  5  mV  s−1  was  recorded  to  identify  the  battery  and  pseudocapacitive

39

38	behavior. The reversible redox peaks (2.35/1.89 V at 0.2 mV s−1) corresponds to

40

41	the  phase  transition  during  Li+  intercalation/de-intercalation,  indicating  the

42

43	charge  storage  mechanism  depends  on  the  diffusion-controlled  reaction  (Fig.

44

45	4a).  The  area  of  CV  curves  increases  with  the  increases  of  scanning  rate,

46

47	accompanied by positive voltage shifts of anodic potential and negative voltage

48

49	shifts  of  cathodic  potential,  respectively.  Consequently,  the  well-matching

50

52

51	concept of  electrodes contributes to the  conspicuous position repeatability of

54

53	CV peaks and electrochemical reversibility of the electrode reaction [25]. The

56

55	calculated-b  values  ranging  from  0.5  to  1.0  indicate  the  “transition”  area

57

58	between the surface-controlled process of pseudocapacitive materials and the

59

60	diffusion-controlled   process   of   battery-type   materials,   and   the   capacitive

1	contribution  increases  with  the  increasing  of  b-values  [27,  28].  The  higher

2

3	b-value  of  anode  (0.73)  and  cathode  (0.61)  reflect  a  mixed  contribution  of

4

5	diffusion-controlled  and  the  surface-controlled  process  (Fig.  4b).  The  higher

6

7	capacity   contribution   (approximately   53.4%)   (Fig.	4c)   of   HESDs   after

8

9	prelithiation  at  a  high  scanning  rate  of  5  mV  s−1  can  be  attributed  to  the

10

11	pseudocapacitive  behavior  of  mFe3C@GO  NSs.  Hence,  the  charge  storage

12

13	mechanism	of	mFe3C@GO	NSs	supercapacitor	is	predominantly	the

14

16

15	surface-controlled   process.   This   is   done   by   adsorbing   and   electrostatic

18

17	accumulating  charges  in  hierarchical  mesoporous  conductive  network  of  GO

20

19	nanosheet,  resulting  in  higher  energy  density  without  the  sacrifice of  power

21

22	density of HESDs after prelithiation. During the charging/discharging process,

23

24	Li+  ions  extracted/inserted  from/into  batter-type  mLVP/C  MSs  electrode  and

25

26	inserted/extracted  into/from  the  mFe3C@GO  NSs  pseudocapacitive  electrode

27

28	by the mechanisms of adsorption and electrostatic accumulation (Fig. 4e). The

29

30	LVP NPs promote the fast Li+ solid-state transportation effectively (Fig. 4d) and

31

32	achieve a high diffusion rate and energy density of batter-type mLVP/C MSs

33

35

34	electrode,  which  may  be  related  to  the  well  contacts  of  the  interconnected

37

36	mesoporous  NPs  and  the  electrolyte.  The  flexible  GO  shell  maintains  the

38

39	structural integrity and elastic buffer, resulting in high power density, excellent

40

41	rate   capability  and   cycle   performance   (Fig.   4f).   In  addition,  the   active

42

43	biocarbon network possesses good electronic conductivity. Therefore, selecting

44

45	and optimizing the active material and electrode architecture benefit to acquire

46

47	ultrahigh energy and power densities of HESDs after prelithiation, which has

48

49	great potential for significantly improving fast and efficient energy storage in

50

52

51	the future.

53

## 54	4. Conclusions

55

56

57	In summary, multifunctional mesoporous core-shell mFe3C@GO NSs was

58

59	prepared  by  hydrothermal  synthesis  and  high-temperature  calcination  with

1	high-quality lignins as the organic ligands of Fe(II)/Fe(III)-MOFs precursor and

2

3	the carbon source. The functional groups of lignins and Fe ions catalyze the

4

5	cross-linking of lignins and the formation of GO nanosheet, and the synthesis

6

7	mechanism was proposed. The mFe3C@GO NSs homogeneously dispersed in

8

9	GO conductive network and maintained the structural integrity of the electrode

10

11	in   the   electrochemical   process,   which   exhibited   high   reversible   specific

12

13	capacity,  excellent  rate  capability  and  cycling  stability.  This  elaborate  work

14

16

15	encourages the investigation of biomass waste conversion and utilization and

18

17	the   extensible   exploration   of	multifunctional   materials   for   rechargeable

20

19	batteries.

21

23

22	Declaration of competing interest

24

25	The authors declare no conflict of interest.

26

27

## 28	Acknowledgements

29

30

31	This work is supported by the National Natural Science Foundation of China

32

33	(No. 61368007), the Natural Science Foundation of Shandong Province (Grant

34

35	No. ZR2019MEM053), and the Project (D20015).

36

37

38	References

39

40

41	1 Su  F,  Qin  J,  Das  P,  Zhou  F,  Wu  ZS.  A  high-performance  rocking-chair

42

43	lithium-ion battery-supercapacitor hybrid device boosted by doubly matched

44

45	capacity and kinetics of the faradaic electrodes. Energy Environ Sci 2021; 14:

46

47	2269-2277. https://doi.org/10.1039/D1EE00317H

48

49	2 Tie D, Huang S, Wang J, Ma J, Zhang J, Zhao Y. Hybrid energy storage

50

51	devices: advanced electrode materials and matching principles. Energy Stor

52

54

53	Mater 2019; 21: 22-40. https://doi.org/10.1016/j.ensm.2018.12.018

56

55	3 Sharma R, Kumar H, Kumar G, Sharma S, Aneja R, Sharma AK, Kumar R,

57

58	Kumar P. Progress and challenges in electrochemical energy storage devices:

1	fabrication, electrode material, and economic aspects. Chem Eng J 2023; 468:

2

3	143706. https://doi.org/10.1016/j.cej.2023.143706

4

5	4  Wei H, Huang W, Luo K, Huang Y, Zhong S, Yan D. PVP-assisted synthesis

6

7	of  hollow  Ni0.75Zn0.25Fe2O4    nanospheres  for  lithium-ion  batteries.  Int  J

8

9	Hydrogen	Energy	2023;	48:	20208-20215.

10

11	https://doi.org/10.1016/j.ijhydene.2023.01.303

12

13	5 Qin  G,  Jia  Z,  Li  A,  Sun  S,  Liu  Z,  Zhuang  CL,  Chen  J.  Nitrogen-rich

14

16

15	carbon/SiO2	nanotubes	composites	prepared	by	self-assembly	as

18

17	high-performance anode lithium-ion battery. Int J Hydrogen Energy 2023; 48:

20

19	20208-20215. https://doi.org/10.1016/j.ijhydene.2023.09.201

21

22	6 Zhang S, Wang K, Chen H, Liu H, Yang L, Chen Y, Li H. ZIF-67 derived

23

24	in-situ	grown	NeCo3S4-GN/CNT	interlinked	conductive	networks	for

25

26	high-performance especially cycling stable supercapacitors. Carbon 2022; 194:

27

28	10-22. https://doi.org/10.1016/j.carbon.2022.03.054

29

30	7 Huang X, Qi X, Boey F, Zhang H. Graphene-based composites. Chem Soc Rev

31

32	2012; 41: 666–686. https://doi.org/10.1039/C1CS15078B

33

35

34	8  Solís-Fernández P, Bissett M, Ago H, Synthesis, structure and applications of

37

36	graphene-based 2D heterostructures. Chem Soc Rev 2017; 46: 4572–4613.

38

39	https://doi.org/10.1039/C7CS00160F

40

41	9 Shi J, Wang Y, Du W, Hou Z. Synthesis of graphene encapsulated Fe3C in

42

43	carbon nanotubes from biomass and its catalysis application. Carbon 2016; 99:

44

45	330–337. https://doi.org/10.1016/j.carbon.2015.12.049

46

47	10 Fan X, Peng Z, Ye R, Zhou H, Guo X. M3C (M: Fe, Co, Ni) nanocrystals

48

49	encased	in	graphene	nanoribbons:	an	active	and	stable	bifunctional

50

52

51	electrocatalyst for oxygen reduction and hydrogen evolution reactions. ACS

54

53	Nano 2015; 9: 7407–7418. https://doi.org/10.1021/acsnano.5b02420

56

55	11 Zhang J, Wang  K,  Xu  Q,  Zhou  Y,  Cheng  F,  Guo  S.  Beyond  yolk-shell

57

58	nanoparticles: Fe3O4@Fe3C  core@shell  nanoparticles  as  yolks  and  carbon

1	nanospindles as shells for efficient lithium ion storage. ACS Nano 2015; 9:

2

3	3369–3376. https://doi.org/10.1021/acsnano.5b00760

4

5	12 Tan Y, Zhu K, Li D, Bai F, Wei Y, Zhang P. N-doped graphene/Fe–Fe3C

6

7	nano-composite synthesized by a Fe-based metal organic framework and its

8

9	anode performance in lithium ion batteries. Chem Eng J 2014; 258: 93–100.

10

11	https://doi.org/10.1016/j.cej.2014.07.066

12

13	13 Zheng J, Kong F, Tao S, Qian B. A Fe2O3-Fe3C heterostructure encapsulated

14

16

15	into a carbon matrix for the anode of lithium-ion batteries. Chem Commun

18

17	2021; 57: 8818-8821. https://doi.org/10.1039/D1CC03945H

20

19	14 Chen R, Zhou Y, Li X. Cotton-derived Fe/Fe3C-encapsulated carbon nanotubes

21

22	for high-performance lithium-sulfur batteries. Nano Lett 2022; 22: 1217–1224.

23

24	https://doi.org/10.1021/acs.nanolett.1c04380

25

26	15 Shen W, Kou W, Liu Y, Dai Y, Zheng W, He G, Wang S, Zhang Y, Wu X,

27

28	Fan S, Li X. Fe3C-doped asymmetric porous carbon membrane binder-free

29

30	integrated materials as high performance anodes of lithium-ion batteries. Chem

31

32	Eng J 2019; 368: 310–320. https://doi.org/10.1016/j.cej.2019.02.199

33

35

34	16 Schlee P, Hosseinaei O, O' Keefe CA, Mostazo-Lopez MJ, Cazorla-Amoros D,

37

36	Herou S, Tomani P, Grey CP, Titirici MM. Hardwood versus softwood Kraft

38

39	lignin-precursor-product relationships in  the  manufacture  of porous  carbon

40

41	nanofibers	for	supercapacitors.	J	Mater	Chem	A	2020;	8:	23543.

42

43	https://doi.org/10.1039/D0TA09093J

44

45	17 Schutyser W, Renders T, Bosch SV, Koelewijn SF, Beckham GT, Sels BF.

46

47	Chemicals	from	lignin:	an	interplay	of	lignocellulose	fractionation,

48

49	depolymerisation,  and   upgrading.  Chem   Soc  Rev   2018;  47:   852–908.

50

52

51	https://doi.org/10.1039/C7CS00566K

54

53	18 Xu YH, Zhou  Q,  Li  MF,  Bian  J,  Peng  F.  Tetrahydro-2-furanmethanol

56

55	pretreatment of eucalyptus to enhance cellulose enzymatic hydrolysis and to

57

58	produce	high-quality	lignin.	Bioresour	Technol	2019;	280:	489–492.

59

60	https://doi.org/10.1016/j.biortech.2019.02.088

1	19 Du X, He W, Zhang X, Yue Y, Liu H, Zhang X, Min D, Ge X, Du Y.

2

3	Enhancing  the  electrochemical  performance  of  lithium  ion  batteries  using

4

5	mesoporous Li3V2(PO4)3/C microspheres. J Mater Chem 2012; 22: 5960–5969.

6

7	https://doi.org/10.1039/C1JM14758G

8

9	20 Fei Y, Liang M, Yan L, Chen Y, Zou H. Co/C@cellulose nanofiber aerogel

10

11	derived from metal-organic frameworks for highly efficient electromagnetic

12

13	interference	shielding.	Chem	Eng	J	2020;	392:	124815.

14

16

15	https://doi.org/10.1016/j.cej.2020.124815

18

17	21 Liu C, Huang X, Liu J, Wang J, Chen Z, Luo R, Wang C, Li J, Wang L, Wang

20

19	J,  Yu  C.  A  general  approach  to  direct  growth  of  oriented  metal-organic

21

22	framework nanosheets on reduced graphene oxides. Adv Sci 2020; 7: 1901480.

23

24	https://doi.org/10.1002/advs.201901480

25

26	22 Han D, Zhao Z, Xu Z, Wang H, He Z, Wang H, Shi J, Zheng L. Metal organic

27

28	frameworks enabled multifunctional poly(ethylene oxide)-based solid polymer

29

30	electrolytes with high lithium-ion conductivity and excellent stability. ACS

31

32	Appl	Energy	Mater	2022;	5:	8973–8981.

33

35

34	https://doi.org/10.1021/acsaem.2c01461

37

36	23 Zhang C, Hu W, Jiang H,  Chang  JK,  Zheng  M,  Wu  QH,  Dong  Q.

38

39	Electrochemical performance  of  MIL-53(Fe)@RGO  as  an  organic  anode

40

41	material	for	li-ion	batteries.	Electrochim	Acta	2017;	246:	528–535.

42

43	https://doi.org/10.1016/j.electacta.2017.06.059

44

45	24 Liang R, Shen L, Jing F, Qin N, Wu L. Preparation of MIL-53(Fe)-reduced

46

47	graphene oxide  nanocomposites  by  a  simple  self-assembly  strategy  for

48

49	increasing interfacial contact: efficient visible-light photocatalysts. ACS Appl

50

52

51	Mater	Interfaces	2015;	7:	9507–9515.

54

53	http://dx.doi.org/10.1021/acsami.5b00682

56

55	25 Zhang H, Cheng J, Liu H, Li D, Zeng Z, Li Y, Ji F, Guo Y, Wei Y, Zhang S,

57

58	Bai T, Xu X, Peng R, Lu J, Ci L. Prelithiation: a critical strategy towards

1	practical application of high-energy-density batteries. Adv Energy Mater 2023;

2

3	13: 2300466. https://doi.org/10.1002/aenm.202300466

4

5	26 Wang F, Wang B, Li J, Wang B, Zhou Y, Wang D, Liu H, Dou S. Prelithiation:

6

7	a  crucial strategy  for  boosting  the  practical  application  of  next-generation

8

9	lithium	ion	battery,	ACS	Nano	2021;	15:	2197–2218.

10

11	https://doi.org/10.1021/acsnano.0c10664

12

13	27 Liu J, Wang J, Xu C, Jiang H, Li C, Zhang L, Lin J, Shen JL. Advanced energy

14

16

15	storage devices: basic principles, analytical methods, and rational materials

18

17	design. Adv Sci 2018; 5: 170032. https://doi.org/10.1002/advs.201700322

20

19	28 Zhang L, Zhang X, Tian G, Zhang Q, Knapp M, Ehrenberg H, Chen G, Shen Z,

21

22	Yang G, Gu L, Du F. Lithium lanthanum titanate perovskite as an anode for

23

24	lithium	ion	batteries.	Nat	Commun	2020;	11:	3490.

25

26	https://doi.org/10.1038/s41467-020-17233-1

27

28

29

30

31

32

33

34

35

36

37

38

39

40

41

42

43

44

45

46

47

48

49

50

51

52

53

54

55

56

57

58

Revised Manuscript (Clean, unmarked, FINAL version)	Click here to view linked References

# Biomass-derived mesoporous core-shell Fe3C@graphene

- oxide nanospheres for electrochemical energy storage

3

4	Xinli Yi,a,b Wen He,c* Xudong Zhang,c Kwan San Huid and Wangwang Xua*

5

- a.College of Materials and Chemical Engineering, Key Laboratory of Inorganic

- Nonmetallic Crystalline and Energy Conversion Materials, China Three Gorges

- University, Yichang, 443002, P. R. China

- b.Hubei Three Gorges Laboratory, Yichang, Hubei 443007, P. R. China.

- c.Department of Materials Science and Engineering, Qilu University of Technology

- (Shandong Academy of Sciences), Jinan, 250353, P. R. China.

- d.School of Engineering, Faculty of science, University of East Anglia, Norwich, NR4

- 7TJ, United Kingdom.

14

## Abstract

- The biomass-derived mesoporous core-shell Fe3C@graphene oxide nanospheres

- (mFe3C@GO NSs) was synthesized with high-quality lignins and applied for

- electrochemical energy storage. The synthesis conditions of mFe3C@GO NSs are

- optimized and   its formation   mechanism   is   proposed.   The mFe3C@GO   NSs

- homogeneously dispersed in GO conductive network and maintained the structural

- integrity of the electrode during the electrochemical process. Benefiting from the

- advantages   of   the   core-shell   construction   and   graphene   oxide   network,   the

- mFe3C@GO NSs exhibits extensible exploration in electrochemical energy storage

- (EES).

- Keywords:	mFe3C@GO	NSs;	Biomass-derived	compounds;	Nanostructured

- electrode; Lithium-ion battery; Electrochemical energy storage

27

28

## 1. Introduction

- Energy storage technology is a frontier research orientation, which efficiently

- eliminates greenhouse gas emissions, reduces petroleum reliance and facilitates

- the sustainable utilization of energy. In order to enhance the competitiveness of

- the rechargeable batteries-based electric vehicles (EVs), some barriers of high

- energy/power density, cost, fast charging capability and compatible sizes need

- to overcome  to  consummate  power  sources  [1-3].  The  integrated  device

- combined with  the advantages of two energy storage  mechanisms,  lead  to a

- “double high”  Li-ion  battery  (LIB)  and  supercapacitor  (SC)  hybrid  energy

- storage   devices   (HESDs),   further   providing   possible	power  source   for

- multi-function   electronic   equipment   and	electric/hybrid   vehicles	[4,  5].

- However, the  mismatches  of  charge  storage  capacity  and  electrode  kinetics

- between battery-type and capacitive electrodes lead to a relatively restricted

- performance of LIB-SC HESDs. [4]. Therefore, the design of high-performance

- electrode materials  and  understanding  on  the  matching  theory  between  the

- positive  and   negative   electrodes   of   LIB-SC   HESDs   face   overwhelming

- challenges [6].

- In	the	pursuit	of	high-performance	energy	storage	devices,

- biomass-derived carbon  materials  and  its  hybrids  have  been  regarded  as  the

- potential candidate electrodes owing to the inexpensive feedstock, nontoxicity

- and diverse  sources  of  renewable  biomass  source  [7,  8].  The  utilization  of

- biomass contributes to achieve a zero-waste circular bioeconomy and greener

- energy storage.  Furthermore,  the  chemical/physical  properties  and  structural

- advantages have  an  effect  on  fabricating  biomass-derived  activated  carbon

- during the following carbonization and activation, resulting in high specific

- surface  area,   pore   structure,   and   high   graphitization   [9,   10].   Especially

- graphene (GN)-like two-dimensional materials, has draws significant attentions

- owing to the unique interfacial structure, attractive properties, facile synthesis,

- and ease  of  functionalization  [11-13].  Numerous  studies  indicate  that  the

- effective work function of carbon-based electrode was increased significantly

- by inserting metal oxide nanoparticles [14-19]. The graphitic carbon and iron

- carbide (Fe3C) bifunctional oxygen electrodes demonstrated synergistic effects

- [20, 21]. For Fe3C anode materials used in LIBs, particularly in high current

- density, there is an urgent need to restrain the structure collapse originated from

- volume  change  during  the  continuous  charge/discharge  process  and  the  poor

- conductivity of Fe3C, which results in rapid capacity fading [22]. Structure

- engineering and conductive network had wide applicability to solve these

- problems [23-25]. Nevertheless, the core-cell carbon coating featured with large

- specific surface area, excellent conductivity and mechanical flexibility can be

- fabricated  through  different  design  strategies, further  contributes to  restricted

- performance improvement [26]. In general, the core-shell structure is desirable

- to realize  synergism  effect,  but  surprisingly  little  attention  focus  on  the

- utilization of lignin. Lignin emerges as a by-product from papermaking industry

- by the degradation of the nature wood, which is suitable for thermochemical

- reaction for its high yield of pyrolysis products and is considered a promising

- feedstock for  carbon  materials  production  [27,  28].  Its  surfactant  structure

- contains multifarious  functional  groups  (carboxyl,  hydroxyl,  benzyl  alcohol,

- methoxyl e.g.) and trace elements (such as Si and S, etc), providing lone pair

- electrons, nucleation sites and adsorb metal ions [29].

- Here, the biomass-derived mesoporous core-shell Fe3C@graphene oxide

- nanospheres (mFe3C@GO  NSs)  were  fabricated  by  a  simple  wet  chemical

- route with high-quality lignins as the organic ligands and the carbon source, and

- the synthesis  mechanism  was  proposed.  The  structure  of  mFe3C@GO  NSs

- exhibits effects on fast ion insertion/extraction, high electrolyte permeability,

- and	electric	conductivity	for	lithium-ion	battery	and	supercapacitor,

- respectively. More importantly, the HESDs constructed with mFe3C@GO NSs

- and mesoporous Li3V2(PO4)3/C microspheres (mLVP/C MSs)  [30] exhibit

- highly matched capacity and significant pseudocapacitive behavior.

## 2. Experiments sections

- 2.1. Synthesis of mFe3C@GO NSs

- The Fe-species composite precursor was synthesized by a simple, low-cost and green

- method of hydrothermal crystallization and reduction. 0.89 g FeCl3·6H2O powder was

- dissolved in 33 mL deionized water  with continuous stirring  to form a uniform

- solution. Then, the solution was slowly added into 50 mL lignin solution (pH ≈ 13)

- with magnetic stirring for 6 h at room temperature to form a thick liquid (pH ≈ 7).

- Subsequently, the thick liquid was then transformed into a Teflon-sealed autoclave

- and heated at 180°C for 48 h. After the autoclave cooled down to room temperature

- naturally, the precipitate was washed with deionized water for three times and dried at

- 60 °C to obtain the Fe-species composite precursor (including Fe3O4 and MIL-53(Fe)).

- Finally, the Fe-species composite precursor was placed in a tube furnace and then

- heated at 800 °C for 8  h with a heating rate  of 5°C min−1 under nitrogen (N2)

- atmosphere. The mFe3C@GO NSs was obtained. For comparison, the GO blank

- sample was prepared by calcination treatment of dried lignin solution at 800 °C under

- N2 for 8 h.

## 2.2. Characterizations

- The crystalline characteristics of materials were identified by X-ray diffraction (XRD,

- LabX XRD-6100) with Cu-Kα radiation (Shimadzu, λ= 1.5406 nm) at a scanning rate

- of 5° min−1. The elemental composition and chemical states of elements was carried

- out by X-ray photoelectron spectroscopy (XPS, ESCALAB Xi+). The binding

- energies were calibrated to the C 1s peak (284.6 eV). The morphologies and surface

- microstructures of materials were observed by Field emission gun (FEG) scanning

- electron microscopy (SEM) (Quanta 200F) using an operating voltage of 20 kV with

- an X-ray energy dispersive spectrometer (EDS) and a ZEISS scanning electron

- microscope. The EDS images were captured at the positions emerged in the TEM

- images, providing the distribution of elements. The crystallographic structure of

- materials were investigated by transmission electron microscopy (TEM, JEF-2100F)

- under the condition of 200 kV. The high-revolution TEM images associated with line

- scanning TEM-EDS profiles indicated the element distribution across the diameter of

- a single nanoparticle. Raman spectra were measured by a Renishaw RM2000 Raman

- microscope with 514 nm excitation argon laser. Differential scanning calorimetry

- (DSC-100H, Nanjingdazhan) was used to measure the thermal change of Fe-species

- composite precursor. Gravimetric analysis is a quantitative chemical method for

- accurately determining the element contents of the materials. The N2 adsorption–

- desorption isotherms and Barrett–Joyner–Halenda (BJH) pore size distribution curves

- were obtained at 77 K using an automatic surface area analyzer (Micromeritics,

- Gemini V2380, USA).

## 2.3. Electrochemical measurements

- 2.3.1 Electrode preparation for LIBs and electrochemical measurements

- The electrochemical performances were characterized in a coin-type LIR2032 cell at

- room temperature. The working electrode was prepared by mixing 80% mFe3C@GO

- NSs, 10% acetylene black and 10% polyvinylidene fluoride (PVDF) in N-methyl

- pyrrolidone, then stirring to prepare the slurry and coating it on copper foil surface

- uniformly. After that, the electrode was dried at 60 °C in an electric thermostatic

- drying oven and then dried at 110 °C for 10 h in vacuum drying oven. The electrode

- was cut it into wafers with a diameter of 15 mm. The average mass loading of the

- mFe3C@GO NSs electrode was about 1.2 mg cm−2 (Table S1). The cells were

- assembled in a high-purity argon-filled inert glove box with the synthesized electrode

- as anode and polypropylene (PP) membrane as a separator, 1.0 M LiPF6 EC: DC:

- EMC (ethylene carbonate: dimethyl carbonate: cthylene methyl carbonate = 1:1:1 ) as

- the	electrolyte.	After	assembling	battery	pack	and	ageing	treatment,	the

- electrochemical characteristics were conducted. The charge-discharge and cyclic

- voltammetry (CV) curves were measured by Channels battery analyzer (CT3008W)

- between 0.01–3.00 V. Electrochemical impedance spectroscopy (EIS) tests were

- performed in the frequency range from 100 KHz  to 10 mHz. The CV and EIS

- measurements were recorded on a PARSTAT 2263 electrochemical workstation. All

- the processes were measured at room temperature.

## 2.3.2 Electrochemical measurements of HESDs

- HESDs were constructed using mFe3C@GO NSs as the anode and mLVP/C MSs as

- the cathode. The experimental process of prelithialization in form is similar to the

- structure of the common half-cell. Before the construction of full battery, the electrode

- materials (anode and cathode) were activated respectively in corresponds half-cell

- systems through electrochemical prelithialization. Afterwards, the half-cell was

- disassembled respectively,   and   then   the   anode   and   cathode   electrodes   were

- reassembled to construct a new full-cell without washing. The average mass loading

- of the mLVP/C MSs cathode was about 1.35 mg cm−2. The charge-discharge curves

- were carried out between 0.00–4.00 V. All the tests were performed at room

- temperature.

- The average mass loading of the active material is shown in equation 1:

- Mass load = m/A	1

- Where m (mg) is the mass of active material, A (cm2) is the area of the electrode

- sheet with a diameter of 15 mm.

## 3. Results and discussion

- Lignin	carbon-based	composites	employ	as	electrode	materials	for

- electrochemical because  of  their  inherited  outstanding  properties  [31,  32].

- Lignin	exhibits	advantages	for	carbon-based	composites	such	as

- environmentally friendly, good biocompatibility, and high carbon content [33].

- Particularly, the functional groups of lignin play key roles in the formation of

- Fe-species precursor. The in-situ synthesis of mFe3C@GO NSs is shown in Fig.

- 1. Benefiting from Fe3+ ions and functional groups in lignin, the nucleation and

- growth of the lyotropic liquid crystals is determined (Fig. S1a). Moreover, the

- factor affecting the spontancous chelation and depolymerization is electrophilic

- attack of lignins (Fig. 1a). The nucleation and growth of Fe3+ ions are correlated

1

- Fig. 1  (a-c)  Schematic  illustration  for  reaction  of  lignin  with  Fe3+.  (d,  e)

- Secondary  building   units   of   Fe(III)-precursor,   Fe(II)/Fe(III)-precursor   and

- Fe-species composite precursor (gray: C; voilet: FeO6 octahedron; blue: FeO4

- tetrahedron). (f) Structure illustrations of mFe3C@GO NSs after carbonization.

6

- with the functional groups and highly hydrophilic groups on lignin surface (Fig.

- 1b). When Fe3+ ions are deficient, the Fe/lignin chelates tend to curl in some

- directions because  of  electrostatic  attraction  (Fig.  1c).  The  hydrothermal

- crystallization	behaviour	of	Fe(III)-precursor	is	associated	with	the

- self-assembly of Fe/lignin chelates. Surplus functional groups were pulled away

- from the lignin structure and donated electron, causing the oxidation-reduction

- reactions of Fe3+ ions and forming the Fe(II)/Fe(III)-precursor, and ultimately

- formed the intermediate Fe-species composite precursor (including Fe3O4 and

- MIL-53(Fe)) (Fig. 1d and e). In the synthesis process, the Fe3O4 produces

- chemisorption	to	the	π	bond	of	unsaturated	hydrocarbons	in	lignin,

- consequently weakening the bond energy of lignin and prompting the cleavage

- of organo-functional  groups  (C-H  and  C-O  bonds).  Meanwhile,  the  lignins

- provide carbon-rich matrix and abundant free carbon atoms. The mFe3C@GO

- NSs was obtained by carbonizing Fe-species composite precursor at 800 °C for

- 8 h in N2 atmosphere. Fe3C nanospheres that coated by graphene oxide are

22

1

- Fig. 2 (a) Local semi-transparent 3D visualisation image and (b) XRD patterns

- of Fe-species composite precursor (black) and simulated MIL-53(Fe) (red). (c)

- XRD patterns of calcined samples at different temperatures. (d) Raman spectra

- of mFe3C@GO  NSs  and  blank  GO  samples.  (e)  TEM  image  and  (f)  the

- elemental mapping image of Fe element. (g) TEM image and TEM-EDS line

- scan curves  along  the  diameter  (the  yellow  line)  of  the  mFe3C@GO  NSs

- nanoparticle.

9

- dispersed	in	the	conductive	network	of	graphitic	carbon	nanosheet

- homogeneously (Fig. 1f).

- X-ray diffraction  (XRD)  patterns  of  the  samples  synthesized  with  the

- different addition amounts of Fe3+ were displayed in Fig. S2, demonstrating the

- optimal volume ratio 0.66 of 1mol L−1 Fe3+ solution and the lignin liquid. The

- semi-transparent 3D visualisation image in Fig. 2a shows the layered skeleton

- structure and open interlinking pores of Fe-species composite precursor with

- oversize connected  pores  (0.5–1.0  μm)  (Fig.  S3).  As  shown  in  Fig.  2b,  the

- phase constitution of the product after hydrothermal treatment was performed

- by X-ray diffraction (XRD). The diffraction peaks at 5-30° correspond to the

- simulated MIL-53(Fe), while the peaks at 30-80° relate to the Fe3O4 crystalline

- phase (JCPDS, No. 89-3854) [34, 35]. The synthetic temperature of Fe3C range

- from 750 to 850 °C was confirmed by differential scanning calorimeter (DSC,

- Fig. S4). The mFe3C@GO NSs synthesized at 800 °C for 8 h is well indexed to

- orthorhombic phase of Fe3C (PDF#65-2413) and graphene oxide, while the

- samples synthesized at 750 °C and 900 °C contain impurity phase (Fig. 2c).

- The  graphene  oxide with  a  high  degree  of disorder  is  evidenced by  a  wide

- reflection  2θ  range  from  20  to  30°,  in  conjunction  with  a  strong  peak

- characteristic at 2θ=25°. The Raman spectra of the mFe3C@GO NSs and blank

- GO samples are revealed in Fig. 2d, which offer more insight into the carbon

- structures and the degree of graphitization. Two prominent characteristic D and

- G peaks for at 1354/1351 cm−1 and 1578/1599 cm−1 are observed, and the

- intensity ratio of ID/IG are 0.54 and 0.94 for the mFe3C@GO NSs and blank GO

- samples, respectively. The relative lower intensity ratio (ID/IG) of mFe3C@GO

- NSs demonstrates a higher graphitization degree of carbon [36]. Furthermore,

- the intense 2D band at 2969 cm−1 corresponds to the two phonons lattice

- vibration, indicating the characteristic of graphene oxide. These results revealed

- the	successful	carbonization	and	graphitization	of	lignins	during	the

- carbonization process [37].

- X-ray photoelectron  spectroscopy  (XPS) was  carried  out to  characterize

- the elemental components and chemical states of mFe3C@GO NSs (Fig. S5a).

- High resolution XPS spectrum of Fe 2p present two signals at 711.5 eV (Fe

- 2p2/3) and 726.0 eV (Fe 2p1/2), declaring Fe (+1) is in a CFe6 octahedron

- environment (Fig. S5b) [24, 25]. The typical C-C peak and C=C peak at 284.8

- eV and 285.4 eV can be ascribed to the GO layer (Fig. S5c). The high-ordered

- GO nanosheets  was  formed  by  cross-linking  condensation  polymerization  of

- lignin molecules during the heat treatment process.

- The blank sample demonstrates the existence of GO and microcomponent

- of SiC (Fig. 2c), in conjunction with a porous sponge structure (Fig. S6), in

- which graphene  oxide  nanosheet  interwined  closely  with  amorphous  carbon

- and graphite carbon nanofibers. The 3D honeycomb structure of mFe3C@GO

- NSs (Fig.  S7)  composed  of  overlap  nanosheets  and  nanospheres  exhibits

- similar morphology to Fe-species composite precursor, illustrating the structure

- stabilization	without	collapse	during	calcination	process	owing	to	its

- thermostability. TEM images (Fig. S8a-c) confirm the dispersed distribution of

- Fe3C nanosphere (10-100 nm), in a typical core-shell configuration that the

- thickness of graphene oxide shell is approximately 4.0 nm. The lattice fringe

- (0.33 nm) of the outer layer of mFe3C@GO NSs relates to the (110) plane of

- graphene oxide, which is in consistent with the results of XRD and Raman

- spectra (Fig. S8d). Moreover, the lattice spacings of 0.20 and 0.24 nm are in

- conformity to the (031) and (210) planes of Fe3C, respectively (Fig. S8e and f).

- The elemental  mapping  images  of  mFe3C@GO  NSs  indicate  the  weight

- percentage  of  Fe  is  approximately  43%  (Fig.  2e  and  f).  Similar  results  was

- conducted by the gravimetric method, with Fe and C contents of 43.4 wt.% and

- 52.2  wt.%,  respectively  (Table  S2).  The  elemental  line  scanning  (Fig.  2g)

- reveals that the Fe element reduced gradually from core to surface along the

- diameter of mFe3C@GO NSs nanosphere, further verifying the inner core of

- Fe3C NPs are well coated by GO shells and homogeneously dispersed in the

- conductive network  of  GO  nanosheet  (Fig.  S9).  Furthermore,  the  increased

- intensity of ordered hierarchical mesopores conduces to improve physical and

- chemical properties of mFe3C@GO NSs. Most notably, the mFe3C@GO NSs

- exhibit an  ultra-high  BET  surface  area  of  639.1  m2  g−1,  promoting  the

- permeability  of   electrolyte   and   resulting   in   an   excellent   electrochemical

- performance (Fig. S10).

- Particularly, the  mFe3C@GO  NSs  synthesized  at  800  °C  delivers  an

- ultrahigh initial discharge and charge capacities of 1800 mAh g−1 and 698.8

- mAh g−1 with initial coulombic efficiency of 38.8% at the current density of 1 A

- g−1 (Fig.  S11).  The  mFe3C@GO  NSs  electrode  delivers  relatively  stable

- discharge/charge capacities  and  Coulombic  efficiency  of  approximately  93%

- from 20th to 50th cycles, demonstrating its excellent cycling stability (Table

1

- Fig. 3 (a) Rate capability of electrodes synthesized at different temperature. (b)

- Cycling performance and Columbic efficiency of mFe3C@GO NSs. (c) Cyclic

- voltammogran curves  at  the  scan  rate  of  0.1  mV  s−1.  Electrochemical

- performance	evaluation	of	HESDs	with	the	optimal	mass	ratio	of

- mpositive/mnegative=4.15. (d, e) Brightness contrast photos of LED bulb driven by

- HESDs, (f) Rate performance, (g) Long-term cycling performance, (h) Nyquist

- plots and (i) Ragone plots.

9

- S3). TEM images in Fig. S12 demonstrate the structural integrity and dispersion

- of mFe3C@GO NSs after 50 cycles. From the structural view, the graphene

- oxide outer layer contributes to restrain excessive side reactions and cushion the

- structural changes  during  the  charging/discharging  process,  resulting  in

- structural integrity. As shown in Fig. 3a, the mFe3C@GO NSs demonstrates

- superior rate  capability  than  that  of  other  anodes  for  lithium-ion  battery.

- Furthermore, the mFe3C@GO NSs exhibits high capacity retention rate after

- 1000 cycles (715 mAh g−1) and approximately 100% Coulombic efficiency

- even at  a  high  current  density  of  10  A g−1  (Fig.  3b),  demonstrating  the

- outstanding  cycling   stability.   Fortunately,   the   mFe3C@GO   NSs   exhibits

- comparable electrochemical performance with the recently reported Fe3C-based

- electrode	materials	(Table	S4)	and	Fe-based	materials	with

- nanosphere-structure	(Table	S5).	The	electrochemical	performance	of

- mFe3C@GO NSs can be attributed to the following factors: (1) The ultra-high

- BET surface area provides abundant active sites and flexible buffer space for

- Li+ storage,  and  the  core-shell  structure  cushions  the  volume  expension

- effectively [38]; (2) The conductive channel between Fe3C and graphitic carbon

- layer improves the electrical conductivity; (3) The graphene oxide outer layer is

- conducive to the adsorption of lithium ion [39].

- The prominent decreased peak intensity at 0.8 V after 1000th cycle and the

- disappeared peak at 1.5 V can be related to the irreversible side reactions and

- the solid electrolyte interface (SEI) formation, respectively (Fig. 3c). The EIS

- plots of  mFe3C@GO  NSs  electrode  before  and  after  cycling,  and  the

- corresponding equivalent  circuit  are  shown  in  Fig.  S13.  The  semicircle  at

- high-frequency areas is relevant to the charge transfer resistance (Rct) on the

- electrode/electrolyte interface,  which  is  parallel  to  the  interface  capacitance

- (CPE). The  oblique  line  at  low-frequency  areas  presents  the  Lithium-ion

- diffusion	impedance	(Warburg	impedance,	Zw).	Obviously,	the	smaller

- semicircular diameters  of  mFe3C@GO  NSs  electrode  after  1000th  cycles

- indicates	the	effectively	improved	electron/ion	transport	properties,	in

- accordance with the electronic conductivity [40-42].

- The HESDs were assembled by mFe3C@GO NSs (anode) and mLVP/C

- MSs	(cathode)	to	reveal	the	potential	application.	The	anode/cathode

- prelithiation is  carried  out  to  overcome  the  electrolyte-consuming  problem,

- tuning the electrochemical performance and achieving remarkable energy and

- high power density [43, 44]. By contrast, the luminosity of LED bulb driven by

- HESDs after prelithiation (Fig. 3e) is significantly higher than that of LED bulb

- before prelithiation (Fig. 3d). The HESDs after prelithiation exhibit better rate

- capability	(Fig.	3f).	The	initial	charge	and	discharge	capacities	after

- prelithiation are 544.7 and 528.1 mAh g−1 at 0.1 A g−1, respectively. The

- HESDs after prelithiation deliver excellent rate performance from 1 to 5 A g−1,

- and the discharge capacity of 217.8 mAh g−1 can be remained at 5 A g−1. The

- long-term  cycling  performance  of  HESDs  after  prelithiation  is  improved

- significantly (Fig. 3g) in contrast to that of HESDs before prelithiation, which

- can be attributed to the lower  Rct  (152.7  Ω) (Fig. 3h) and the enhanced

- contribution of  pseudocapacitive  behavior  (Fig.  S14).  Extraordinarily,  the

- HESDs after prelithiation still display a discharge capacity of 136 mAh g−1 and

- a retention rate of 91.6% after 1200 cycles at 5 A g−1. The HESDs after

- prelithiation present ultrahigh energy and power densities (Fig. 3i), exhibiting

- exceptionally matched faradaic capacity and kinetics.

- The synergy effect between cathode and anode was further investigated to

- explore the  energy  storage  mechanism.  CV  curves  of  the  HESDs  after

- prelithiation was  recorded  in  a  voltage  window  of  1.5-3.0  V with  changing

- scanning rate from 0.2 to 5 mV s−1 to identify the battery and pseudocapacitive

- behavior. The reversible redox peaks (2.35/1.89 V at 0.2 mV s−1) corresponds to

- the phase transition during Li+ intercalation/de-intercalation, indicating the

- charge storage  mechanism  depends  on  the  diffusion-controlled  reaction  (Fig.

- 4a). The  area  of  CV  curves  increases  with  the  increasing  of  scanning  rate,

- accompanied by positive voltage shifts of anodic potential and negative voltage

- shifts of  cathodic  potential,  respectively.  Consequently,  the  well-matching

- concept of electrodes contributes to the conspicuous position repeatability of

- CV peaks and electrochemical reversibility of the electrode reaction [43]. The

- calculated-b  values  ranging  from  0.5  to  1.0  indicate  the  “transition”  area

- between the surface-controlled process of pseudocapacitive materials and the

- diffusion-controlled  process   of   battery-type   materials,   and   the   capacitive

- contribution increases with the increasing of b-values [45, 46]. The higher

- b-value of anode (0.73) and cathode (0.61) reflect a mixed contribution of

1

- Fig. 4 (a) CV curves, (b) Plots of log (sweep rate) versus log (peak current) and

- (c) Capacitive contribution of HESDs after prelithiation at various sweep rates.

- (e)  Schematic   diagram   of   energy   storage   mechanisms   of   HESDs   after

- prelithiation. Schematic representation of the microstructure of (d) batter-type

- mLVP/C MSs electrode and (f) mFe3C@GO NSs pseudocapacitive electrode.

7

- diffusion-controlled and  the  surface-controlled  process  (Fig.  4b).  The  higher

- capacity  contribution   (approximately   53.4%)   (Fig.   4c)   of   HESDs   after

- prelithiation at a high scanning rate of 5 mV s−1 can be attributed to the

- pseudocapacitive behavior of mFe3C@GO NSs. Hence, the charge storage

- mechanism	of	mFe3C@GO	NSs	supercapacitor	is	predominantly	the

- surface-controlled  process.   This   is   done   by   adsorbing   and   electrostatic

- accumulating charges  in  hierarchical  mesoporous  conductive  network  of  GO

- nanosheet, resulting  in  higher  energy  density  without  the  sacrifice  of  power

- density of HESDs after prelithiation. During the charging/discharging process,

- Li ions  extracted/inserted  from/into  batter-type  mLVP/C  MSs  electrode  and

- inserted/extracted into/from the mFe3C@GO NSs pseudocapacitive electrode

- by the mechanisms of adsorption and electrostatic accumulation (Fig. 4e). The

- LVP NPs promote the fast Li+ solid-state transportation effectively (Fig. 4d) and

- achieve a high diffusion rate and energy density of batter-type mLVP/C MSs

- electrode, which may be related to the well contacts of the interconnected

- mesoporous NPs  and  the  electrolyte.  The  flexible  GO  shell  maintains  the

- structural integrity and elastic buffer, resulting in high power density, excellent

- rate  capability  and   cycle   performance   (Fig.   4f).   In  addition,  the   active

- biomass-derived carbon layer network possesses good electronic conductivity.

- Therefore,	selecting	and	optimizing	the	active	material	and	electrode

- architecture benefit to acquire ultrahigh energy and power densities of HESDs

- after prelithiation, which has great potential for significantly improving fast and

- efficient energy storage in the future. The insights gained from studying button

- cell-type  electrochemical  cells  contribute  to  advancements  in  energy  density,

- efficiency,  safety,  and  longevity,  which  are  crucial  for  powering  electric

- vehicles with heavy motors. Improving the performance of these smaller cells

- can lead  to  advancements  in  larger  battery technologies,  making  them  more

- reliable, cost-effective, and suitable for high-demand applications like electric

- vehicles.

- Consequently, we  explored  the  methods  to  fabricate  biomass-derived

- electrode materials and its utilization in energy storage devices. The regulation

- of  experimental   conditions   (such   as   raw   material   dosage,   carbonization

- temperature) has enabled development of high performance electrode materials

- from biomass  energy  source.  This  holds  tremendous  potential  for  harvesting

- green	electrode	materials	with	high	performance,	in	conjunction	with

- reutilization process  and  cost  inexpensive.  However,  despite  these  unique

- structural	characteristics	and	high	electrochemical	performance	of

- biomass-derived  electrode   materials,   significant   questions   and   challenges

- remain.  The   chemical   composition,   impurities   and   structure   of   biomass

- feedstock are  affected  by  the  natural  changes,  consequently  resulting  in

- inconstant	internal	structure.	Assume	that	these	factors	associate	with

- performance, further explorations associated with technologies and limitations

- are needed for large-scale applications in energy storage devices.

## 4. Conclusions

- In summary, multifunctional mesoporous core-shell mFe3C@GO NSs was

- prepared by  hydrothermal  synthesis  and  high-temperature  calcination  with

- high-quality lignins as the organic ligands of the intermediate precursor and the

- carbon source. During the carbonization process, the lignins were successfully

- graphitized, and the synthesis mechanism of mFe3C@GO NSs was simulated

- and  proposed.   The   mFe3C@GO   NSs   homogeneously   dispersed   in   GO

- conductive  network  and  maintained  the  structural  integrity  of  the  electrode

- during the electrochemical process, resulting in high reversible specific capacity,

- excellent rate capability and cycling stability. This elaborate work encourages

- the investigation of biomass waste conversion and utilization and the extensible

- exploration of multifunctional materials for rechargeable batteries.

## Declaration of competing interest

- The authors declare no conflict of interest.

## Acknowledgements

- This work is supported by the National Natural Science Foundation of China

- (No. 61368007), the Natural Science Foundation of Shandong Province (Grant

- No. ZR2019MEM053), and the Project (D20015).

## Declaration of generative AI and AI-assisted technologies

- The use of generative artificial intelligence (AI) or AI-assisted technologies in

- this article is not permitted in academic writing process.

## CRediT authorship contribution statement

- Xinli Yi designed and proceed the experiments, performed the analysis, drafted the

- manuscript and designed the figures. Wen He and Wangwang Xu contributed to the

- design and implementation of the research, to the analysis of the results and to the

- reviewing & editing of the manuscript. Xudong Zhang was involved in planing and

- supervised the work. Kwan San Hui aided in interpreting the results and contributed

- to the final version of the manuscript. All authors discussed the results and contributed

- to the final manuscript.

## References

- 1. Deng J, Bae C, Denlinger A, Miller T. Electric vehicles batteries: requirements and

9	challenges. Joule 2020; 4: 509-515. https://doi.org/10.1016/j.joule.2020.01.013

- 2. Kumar H, Sharm R, Yadav A, Kumar R. Recent advancement made in the field of

- reduced graphene oxide-based nanocomposites used in the energy storage devices: A

12	review. J Energy Storage 2021; 33: 102032. https://doi.org/10.1016/j.est.2020.102032

- 3. He W, Li C, Zhao B, Zhang X, Hui K S, Zhu J. Metal Ti quantum chain-inlaid 2D

- NaSn2(PO4)3/H-doped hard carbon hybrid electrodes with ultrahigh energy storage

15	density. Chem Eng J 2021; 403: 126311. https://doi.org/10.1016/j.cej.2020.126311

- 4. Su F, Qin J, Das P, Zhou F, Wu ZS. A high-performance rocking-chair lithium-ion

- battery-supercapacitor hybrid device boosted by doubly matched capacity and kinetics

- of	the	faradaic	electrodes.	Energy	Environ	Sci	2021;	14:	2269-2277.

19	https://doi.org/10.1039/D1EE00317H

- 5. Tie D, Huang S, Wang J, Ma J, Zhang J, Zhao Y. Hybrid energy storage devices:

- advanced electrode materials and matching principles. Energy Stor Mater 2019; 21:

22	22-40. https://doi.org/10.1016/j.ensm.2018.12.018

- 6. Sharma R, Kumar H, Kumar G, Sharma S, Aneja R, Sharma AK, Kumar R, Kumar

- P. Progress and challenges in electrochemical energy storage devices: fabrication,

- electrode material, and economic aspects. Chem Eng J 2023; 468: 143706.

26	https://doi.org/10.1016/j.cej.2023.143706

- 7. Jin C, Nai J, Sheng O, Yuan H, Zhang W, Tao X, Lou X. Biomass-based materials

- for green lithium secondary batteries. Energy Environ Sci 2021; 14: 1326.

3	https://doi.org/10.1039/d0ee02848g

- 8. Baskar A V., Singh G, Ruban A M., Davidraj J M., Bahadur R, Sooriyakumar P,

- Kumar P, Karakoti A, Yi J, Vinu A. Recent progress in synthesis and application of

- biomass-based hybrid electrodes for rechargeable batteries. Adv Funct Mater 2023; 33:

7	2208349. https://doi.org/10.1002/adfm.202208349

- 9. Liang J, Liu X, Zhang T, Yu K, Liang C. Hemp straw carbon and Ni/NiO

- embedded structure composites as anode materials for lithium ion batteries. J Alloys

10	Compd 2021; 889: 161776. https://doi.org/10.1016/j.jallcom.2021.161776

- 10. Park S, Song J, Lee W C, Jang S, Lee J, Kim J, Kim H-K, Min K. Advances in

- biomass-derived electrode materials for energy storage and circular carbon economy.

13	Chem Eng J 2023; 470: 144234. https://doi.org/10.1016/j.cej.2023.144234

- 11. Wei H, Huang W, Luo K, Huang Y, Zhong S, Yan D. PVP-assisted synthesis of

- hollow Ni0.75Zn0.25Fe2O4 nanospheres for lithium-ion batteries. Int J Hydrog Energy

16	2023; 48: 20208-20215. https://doi.org/10.1016/j.ijhydene.2023.01.303

- 12. Qin G, Jia Z, Li A, Sun S, Liu Z, Zhuang CL, Chen J. Nitrogen-rich carbon/SiO2

- nanotubes composites   prepared   by   self-assembly   as   high-performance   anode

- lithium-ion	battery.	Int	J	Hydrog	Energy	2023;	48:	20208-20215.

20	https://doi.org/10.1016/j.ijhydene.2023.09.201

- 13. Yadav A, Kumar H, Sharm R, Kumari R, Singh D, Hamed O A.. Metal oxide

- decorated polyaniline based multifunctional nanocomposites: An experimental and

- theoretical	approach.	Results	in	Engineering	2023;	18:	101161.

24	https://doi.org/10.1016/j.rineng.2023.101161

- 14. Zhang S, Wang K, Chen H, Liu H, Yang L, Chen Y, Li H. ZIF-67 derived in-situ

- grown NeCo3S4-GN/CNT interlinked conductive networks for high-performance

- especially	cycling	stable	supercapacitors.	Carbon	2022;	194:	10-22.

28	https://doi.org/10.1016/j.carbon.2022.03.054

1	15. Huang X, Qi X, Boey F, Zhang H. Graphene-based composites. Chem Soc Rev

2	2012; 41: 666–686. https://doi.org/10.1039/C1CS15078B

- 16. Solís-Fernández P, Bissett M, Ago H, Synthesis, structure and applications of

- graphene-based	2D   heterostructures.	Chem	Soc   Rev   2017;   46:	4572–4613.

5	https://doi.org/10.1039/C7CS00160F

- 17. Kumar H, Luthra M, Punia M, Singh D. Ag2O@PANI nanocomposites for

- advanced functional applications: A sustainable experimental and theoretical approach.

- Colloids	Surf	A	Physicochem	Eng	Asp	2022;	640:	128464.

9	https://doi.org/10.1016/j.colsurfa.2022.128464

- 18. Kumari R, Kumar H,	Sharma R, Yadav A, Kumar G, Tundwal A, Dhayal A,

- Sharma A. Highly sensitive amperometric food sensor for Sudan-I dye using

- nanocomposites modified working electrode. Microchem J 2023; 193: 109078.

13	https://doi.org/10.1016/j.microc.2023.109078

- 19. Yadav A, Kumar H, Sharma R, Kumari R, Kumar G, Tundwal A, Dhayal A, Yadav

- A, Singh   D.   Mixed   metal   oxide   decorated   polypyrrole   nanocomposites   for

- multifunctional	applications.	Inorg.	Chem	Commun	2023;	158:	111701.

17	https://doi.org/10.1016/j.inoche.2023.111701

- 20. Shi J, Wang Y, Du W, Hou Z. Synthesis of graphene encapsulated Fe3C in carbon

- nanotubes from biomass and its catalysis application. Carbon 2016; 99: 330–337.

20	https://doi.org/10.1016/j.carbon.2015.12.049

- 21. Fan X, Peng Z, Ye R, Zhou H, Guo X. M3C (M: Fe, Co, Ni) nanocrystals encased

- in graphene nanoribbons: an active and stable bifunctional electrocatalyst for oxygen

- reduction and hydrogen evolution reactions. ACS Nano 2015; 9: 7407–7418.

24	https://doi.org/10.1021/acsnano.5b02420

- 22. Zhang J, Wang K, Xu Q, Zhou Y, Cheng F, Guo S. Beyond yolk-shell

- nanoparticles:	Fe3O4@Fe3C	core@shell	nanoparticles	as	yolks	and	carbon

- nanospindles as shells for efficient lithium ion storage. ACS Nano 2015; 9: 3369–

28	3376. https://doi.org/10.1021/acsnano.5b00760

- 23. Tan Y, Zhu K, Li D, Bai F, Wei Y, Zhang P. N-doped graphene/Fe–Fe3C

- nano-composite synthesized by a Fe-based metal organic framework and its anode

- performance	in	lithium	ion	batteries.	Chem	Eng	J	2014;	258:	93–100.

4	https://doi.org/10.1016/j.cej.2014.07.066

- 24. Zheng J, Kong F, Tao S, Qian B. A Fe2O3-Fe3C heterostructure encapsulated into a

- carbon matrix for the anode of lithium-ion batteries. Chem Commun 2021; 57:

7	8818-8821. https://doi.org/10.1039/D1CC03945H

- 25. Chen R, Zhou Y, Li X. Cotton-derived Fe/Fe3C-encapsulated carbon nanotubes for

- high-performance	lithium-sulfur	batteries.	Nano	Lett	2022;	22:	1217–1224.

- https://doi.org/10.1021/acs.nanolett.1c04380

- 26. Shen W, Kou W, Liu Y, Dai Y, Zheng W, He G, Wang S, Zhang Y, Wu X, Fan S,

- Li X. Fe3C-doped asymmetric porous carbon membrane binder-free integrated

- materials as high performance anodes of lithium-ion batteries. Chem Eng J 2019; 368:

14	310–320. https://doi.org/10.1016/j.cej.2019.02.199

- 27. Schlee P, Hosseinaei O, O' Keefe CA, Mostazo-Lopez MJ, Cazorla-Amoros D,

- Herou S, Tomani P, Grey CP, Titirici MM. Hardwood versus softwood Kraft

- lignin-precursor-product relationships in the manufacture of porous carbon nanofibers

- for	supercapacitors.	J	Mater	Chem	A	2020;	8:	23543.

19	https://doi.org/10.1039/D0TA09093J

- 28. Schutyser W, Renders T, Bosch SV, Koelewijn SF, Beckham GT, Sels BF.

- Chemicals from lignin: an interplay of lignocellulose fractionation, depolymerisation,

- and	upgrading.	Chem	Soc	Rev	2018;	47:	852–908.

23	https://doi.org/10.1039/C7CS00566K

- 29. Xu YH, Zhou Q, Li MF, Bian J, Peng F. Tetrahydro-2-furanmethanol pretreatment

- of eucalyptus to enhance cellulose enzymatic hydrolysis and to produce high-quality

- lignin.	Bioresour	Technol	2019;	280:	489–492.

27	https://doi.org/10.1016/j.biortech.2019.02.088

28	30. Du X, He W, Zhang X, Yue Y, Liu H, Zhang X, Min D, Ge X, Du Y. Enhancing

- the electrochemical   performance   of   lithium   ion   batteries   using   mesoporous

- Li3V2(PO4)3/C	microspheres.	J	Mater	Chem	2012;	22:	5960–5969.

3	https://doi.org/10.1039/C1JM14758G

- 31. N	Izaguirre,	M	Alberro,	X	Erdocia,	J	Labidi.	Kraft	and	organosolv

- lignin-activated carbon composites for supercapacitor electrode materials. J Energy

6	Storage 2024; 80: 110386. https://doi.org/10.1016/j.est.2023.110386

- 32. M Zhu, H Liu, Q Cao, H Zheng, D Xu, H Guo, S Wang, Y Li, J Zhou. Electrospun

- lignin-based carbon nanofibers as supercapacitor electrodes. ACS Sustainable Chem.

9	Eng. 2020, 8: 12831–12841. https://doi.org/10.1021/acssuschemeng.0c03062

- 33. Y She, X Li, Y Zheng, D Chen, X Rui, X Lin, Y Qin. Natural Lignin: A

- sustainable and cost-effective electrode material for high-temperature Na-ion battery.

- Energy Environ Mater 2022, 0: e12538. https://doi.org/10.1002/eem2.12538

- 34. Zhang C, Hu W, Jiang H, Chang JK, Zheng M, Wu QH, Dong Q. Electrochemical

- performance of MIL-53(Fe)@RGO as an organic anode material for li-ion batteries.

15	Electrochim Acta 2017; 246: 528–535. https://doi.org/10.1016/j.electacta.2017.06.059

- 35. Liang R, Shen L, Jing F, Qin N, Wu L. Preparation of MIL-53(Fe)-reduced

- graphene oxide nanocomposites by a simple self-assembly strategy for increasing

- interfacial contact: efficient visible-light photocatalysts. ACS Appl Mater Interfaces

19	2015; 7: 9507–9515. http://dx.doi.org/10.1021/acsami.5b00682

- 36. Gong Y, Li D, Luo C, Fu Q, Pan C. Highly porous graphitic biomass carbon as

- advanced electrode materials for supercapacitors. Green Chem 2017: 19: 4132.

22	https://doi.org/10.1039/c7gc01681f

- 37. W Qu, X Han, J Liu, L Yin, C Liang, P Hu. Unlocking the graphitization potential

- of lignin: insights into its transformation through hot pressing and carbonization.

25	Green Chem 2023, 25: 9873-9883. https://doi.org/10.1039/D3GC03642A

- 38. Li H, Peng J, Wu Z, Liu X, Liu P, Chang B, Wang X. Constructing novel SiOx

- hybridization materials by a double-layer interface engineering for high-performance

- lithium-ion	batteries.	Chem	Eng	J	2023;	462:	142172.

1	https://doi.org/10.1016/j.cej.2023.142172

- 39. Li W, Peng J, Li H, Wu Z, Chang B, Guo X, Chen G, Wang X. Architecture and

- performance of Si/C microspheres assembled by nanoSi via electro-spray technology

- as stability-enhanced anodes for lithiumion batteries. J Alloys Compd 2022; 903:

5	163940. https://doi.org/10.1016/j.jallcom.2022.163940

- 40. Luo S, Peng L, Xie Y, Cao X, Wang X, Liu X, Chen T, Han Z, Fan P, Sun H, Shen

- Y, Guo F, Xia Y, Li K, Ming X, Gao C. Flexible large‑ area graphene films of 50–600

- nm	thickness	with	high	carrier	mobility.	Nano-Micro	Lett	2023;	15:	61.

9	https://doi.org/10.1007/s40820-023-01032-6

- 41. Peng L, Han Y, Wang M, Cao X, Gao J, Liu Y, Chen X, Wang B, Wang B, Zhu C,

- Wang X, Cao K, Huang M, Cunning B V., Pang J, Xu W, Ying Y, Xu Z, Fang W, Lu Y,

- Ruoff R S., Gao C. Multifunctional macroassembled graphene nanofilms with high

13	crystallinity. Adv Mater 2021; 33: 2104195. https://doi.org/10.1002/adma.202104195

- 42. Zhang M, Guan K, Ji Y, Liu G, Jin W, Xu N. Controllable ion transport by

- surface-charged	graphene	oxide	membrane.	Nat	Commun	2019;	10:	1253.

16	https://doi.org/10.1038/s41467-019-09286-8

- 43. Zhang H, Cheng J, Liu H, Li D, Zeng Z, Li Y, Ji F, Guo Y, Wei Y, Zhang S, Bai T,

- Xu X, Peng R, Lu J, Ci L. Prelithiation: a critical strategy towards practical

- application of high-energy-density batteries. Adv Energy Mater 2023; 13: 2300466.

20	https://doi.org/10.1002/aenm.202300466

- 44. Wang F, Wang B, Li J, Wang B, Zhou Y, Wang D, Liu H, Dou S. Prelithiation: a

- crucial strategy for boosting the practical application of next-generation lithium ion

23	battery, ACS Nano 2021; 15: 2197–2218. https://doi.org/10.1021/acsnano.0c10664

- 45. Liu J, Wang J, Xu C, Jiang H, Li C, Zhang L, Lin J, Shen JL. Advanced energy

- storage devices: basic principles, analytical methods, and rational materials design.

26	Adv Sci 2018; 5: 170032. https://doi.org/10.1002/advs.201700322

- 46. Zhang L, Zhang X, Tian G, Zhang Q, Knapp M, Ehrenberg H, Chen G, Shen Z,

- Yang G, Gu L, Du F. Lithium lanthanum titanate perovskite as an anode for lithium

1	ion	batteries.	Nat	Commun	2020;	11:	3490.

2	https://doi.org/10.1038/s41467-020-17233-1